Photovoltaic Performance Analysis of RbGeI3 Absorber Based Perovskite Solar Cell using SCAPS-1D Simulation

By

Md. Abdul Malek Fahim

BACHELOR OF SCIENCE

IN

ELECTRICAL AND ELECTRONIC ENGINEERING

Department of Electrical and Electronic Engineering

Leading University, Sylhet

June, 2026

# Certificate of Approval

The thesis titled, “Photovoltaic Performance Analysis of RbGeI3 Absorber Based Perovskite Solar Cell using SCAPS-1D Simulation” submitted by Md. Abdul Malek Fahim (Id. 0182220012131004) has been found as satisfactory and accepted as partial fulfillment of the requirement for the degree Bachelor of Science in Electrical and Electronic Engineering on May 18, 2026.

-----------------------------------

Rafiqul Islam (Supervisor)
Assistant Professor
Department of Electrical and Electronic Engineering
Leading University, Sylhet

-----------------------------------

Ishmam Ahmed Chowdhury (Co-Supervisor)
Lecturer
Department of Electrical and Electronic Engineering
Leading University, Sylhet

-----------------------------------

Md. Niaz Morshedul Haque
Assistant Professor
Head of the Department
Department of Electrical and Electronic Engineering
Leading University, Sylhet

# Declaration

This is to clarify that paper is the outcome of accomplishment of the thesis on “Photovoltaic Performance Analysis of RbGeI3 Absorber Based Perovskite Solar Cell using SCAPS-1D Simulation” carried out by the student of Department of Electrical and Electronic Engineering, Leading University, Sylhet. It has not been submitted anywhere for any award, degree or diploma, nor it has been published in any technical journal.

-----------------------------------

Md. Abdul Malek Fahim
Student Id: 0182220012131004

“We dedicate this to our beloved parents, honorable teachers and fellow members without whom it was almost impossible to complete our thesis work and obviously to our country
The People’s Republic of Bangladesh”

# Table of Contents

Certificate of Approval	i

Declaration	ii

Table of Contents	iv

List of Figures	vii

List of Tables	viii

Abbreviation	ix

Acknowledgement	x

Abstract	xi

1	Introduction	1

1.1	Background	1

1.2	Literature Review	3

1.2.1	Research Gap	7

1.3	Thesis Objectives	7

1.4	Thesis Organization	8

2	Theoretical background and working principle	9

2.1	Research Methodology	9

2.2	SCAPS-1D Simulation Tool	10

2.3	Device Structure and Working Principle	12

2.3.1	Transparent Conducting Oxide (FTO)	13

2.3.2	Electron Transport Layer (TiO₂)	14

2.3.3	Absorber Layer (RbGeI₃)	14

2.3.4	Hole Transport Layer (CuI)	15

2.3.5	Back Metal Contact (Au)	15

2.3.6	Working Principle of the Proposed Solar Cell	15

3	Chapter 3: Material selection and parameters	16

3.1	Material selection	16

3.1.1	Selection of Electron Transport Layer (TiO₂)	16

3.1.2	Selection of Absorber Layer (RbGeI₃)	18

3.1.3	Selection of Hole Transport Layer (CuI)	20

3.1.4	Selection of Front Contact (FTO)	22

3.1.5	Selection of Back Contact (Au)	23

3.2	Material Parameters	26

4	Device Configurations and optimization procedure	28

4.1	Device Configuration	28

4.2	Simulation Conditions	29

4.3	Performance Parameters	30

4.3.1	Open-Circuit Voltage (VOC)	31

4.3.2	Short-Circuit Current Density (JSC)	31

4.3.3	Fill Factor (FF)	31

4.3.4	Power Conversion Efficiency (PCE)	32

4.4	Optimization Procedure	32

4.4.1	Optimization of Absorber Layer Thickness	32

4.4.2	Optimization of ETL Thickness	33

4.4.3	Optimization of HTL Thickness	33

4.4.4	Optimization of Dielectric Constant	33

4.4.5	Optimization of Bandgap	34

4.4.6	Optimization of Electron Affinity	34

4.4.7	Optimization of Defect Density	34

4.4.8	Optimization of Interface Defect Density	34

4.4.9	Optimization of Density of States (DOS)	35

4.5	Research Flowchart	36

5	Results and discussion	37

5.1	Effect of the absorber layer thickness	37

5.2	Effect of Absorber layer’s defect density	38

5.3	Effect of absorber layer’s dielectric constant	40

5.4	Effect of absorber layer’s electron affinity	41

5.5	Effect of Absorber/ETL interfacial defect densities	43

5.6	Effect of HTL/Absorber interfacial defect densities	45

5.7	Effect of absorber bandgap	46

5.8	Effect of ETL thinkness	48

5.9	Effect of HTL thickness	50

5.10	Effect of Conduction band effective density of states	52

5.11	Effect of Valence band effective density of states	53

5.12	Quantum Efficiency (QE) Analysis	55

5.13	Energy Band Diagram Analysis of CuI/RbGeI₃/TiO₂/FTO Solar Cell	57

5.14	Summary of Optimized Device Parameters	59

5.15	Experimental Validations and Challenges	60

6	Conclusion and future work	63

6.1	Conclusion	63

6.2	Future Work	64

7	References	67

# List of Figures

Figure 2.1 Graphical user interface of SCAPS-1D (Version 3.3.10) used for device simulation.	12

Figure 2.2 Schematic diagram of the proposed FTO/TiO₂/RbGeI₃/CuI/Au perovskite solar cell structure.	13

Figure 4.1 Sequential optimization procedure adopted in this study using the SCAPS-1D simulation software.	35

Figure 4.2 Overall research methodology adopted in the present study.	36

Figure 5.1 Variation of PCE, VOC, JSC, and FF with absorber layer thickness on device performance	38

Figure 5.2 Variation of PCE, VOC, JSC, and FF with absorber layer defect density	39

Figure 5.3 Variation of PCE, VOC, JSC, and FF with absorber layer’s dielectric constant	41

Figure 5.4 Variation of PCE, VOC, JSC, and FF with absorber layer’s electron affinity	43

Figure 5.5 Variation of PCE, VOC, JSC, and FF with Absorber/ETL interfacial defect densities	44

Figure 5.6 Variation of PCE, VOC, JSC, and FF with HTL/Absorber/ interfacial defect densities	46

Figure 5.7 Variation of PCE, VOC, JSC, and FF with absorber bandgap	47

Figure 5.8 Variation of PCE, VOC, JSC, and FF with ETL thickness	49

Figure 5.9 Variation of PCE, VOC, JSC, and FF with HTL thickness	51

Figure 5.10 Variation of PCE, VOC, JSC, and FF with Conduction band effective density of states	53

Figure 5.11 Variation of PCE, VOC, JSC, and FF with valence band effective density of states	54

Figure 5.12 Variation of quantum efficiency (QE) with incident wavelength of the optimized solar cell.	57

Figure 5.13 Energy band diagram at the HTL/absorber and absorber/ETL interfaces.	59

List of Tables

Table 1.1 Summary of literature review	4

Table 3.1 Justification for the Selection of Materials Used in the Proposed Perovskite Solar Cell	25

Table 3.2 Initial Electrical and Optical Parameters Used in the SCAPS-1D Simulation of the Proposed FTO/TiO₂/RbGeI₃/CuI/Au Solar Cell	27

Table 3.3 Initial Interface Defect Density Used in the SCAPS-1D Simulation	27

Table 4.1 Various device configurations	29

Table 4.2 Simulation conditions used in SCAPS-1D	30

Table 5.1 Variation of PCE, VOC, JSC, and FF with absorber layer thickness on device	37

Table 5.2 Variation of PCE, VOC, JSC, and FF with absorber layer defect density	39

Table 5.3 Variation of PCE, VOC, JSC, and FF with absorber layer’s dielectric constant	40

Table 5.4 Variation of PCE, VOC, JSC, and FF with absorber layer’s dielectric constant	42

Table 5.5 Variation of PCE, VOC, JSC, and FF with Absorber/ETL interfacial defect densities	44

Table 5.6 Variation of PCE, VOC, JSC, and FF with HTL/Absorber/ interfacial defect densities	45

Table 5.7 Variation of PCE, VOC, JSC, and FF with absorber bandgap	47

Table 5.8 Variation of PCE, VOC, JSC, and FF with ETL thickness	49

Table 5.9 Variation of PCE, VOC, JSC, and FF with HTL thickness	50

Table 5.10 Variation of PCE, VOC, JSC, and FF with Conduction band effective density of states	52

Table 5.11 Variation of PCE, VOC, JSC, and FF with valence band effective density of states	54

Table 5.12 Variation of quantum efficiency (QE) with incident wavelength of the optimized solar cell.	56

Table 5.13 Optimized Material Parameters of the Proposed FTO/TiO₂/RbGeI₃/CuI/Au Perovskite Solar Cell	60

Table 5.14 Perovskite solar cell performance at different device structures.	62

# Abbreviation

Table 1: List of Abbreviation

| Abbreviation | Full Form |
| --- | --- |
| PSC | Perovskite Solar Cell |
| ETL | Electron Transport Layer |
| HTL | Hole Transport Layer |
| PCE | Power Conversion Efficiency |
| VOC | Open-Circuit Voltage |
| JSC | Short-Circuit Current Density |
| FF | Fill Factor |
| DOS | Density of States |
| SCAPS | Solar Cell Capacitance Simulator |
| AM1.5G | Air Mass 1.5 Global |
| SRH | Shockley–Read–Hall |

# Acknowledgement

First and foremost, we begin with the utmost gratitude, extending our sincere thanks to the most Powerful, Merciful and the Gracious Almighty Allah for all the countless gifts and for enabling us the Knowledge, Energy, Endurance and Aptitude to successfully complete the thesis paper.

It is a great pleasure to acknowledge our deepest thanks and gratitude to our supervisor Rafiqul Islam, Assistant Professor, Department of Electrical & Electronic Engineering and our co-supervisor Ishmam Ahmed Chowdhury, Lecturer, Department of Electrical and Electronic Engineering, Leading University, Sylhet for their visionary support and unwavering guidance throughout the course of this work.

We would like to express our sincere and profound gratitude to honorable Md. Niaz Morshedul Haque, Assistant Professor and Head of the Department of Electrical and Electronic Engineering, Leading University, Sylhet, for granting us full freedom towards the utilization of all the facilities in the department.

Last but not least, we would like to thank our parents and family members for their unconditional love and continuous support. We would not have been able to complete Thesis without them.

# Abstract

The growing demand for clean and affordable energy has intensified research interest in perovskite solar cells as a third-generation photovoltaic technology. However, the widespread use of lead in conventional perovskite absorbers raises serious environmental and health concerns, prompting the need for lead-free alternatives. This study investigates the photovoltaic performance of rubidium germanium iodide (RbGeI₃) as an eco-friendly perovskite absorber using the SCAPS-1D numerical simulation tool under standard AM 1.5G illumination at 1000 W/m².

Eight device configurations were initially designed by combining two electron transport layers (TiO₂ and PCBM) with four hole transport layers (NiO, CuI, CBTS, and Spiro-OMeTAD), all incorporating RbGeI₃ as the absorber. The configuration D4, corresponding to the FTO/TiO₂/RbGeI₃/CuI/Au architecture, demonstrated the highest initial performance.

A comprehensive parameter study was carried out by varying the absorber thickness, absorber defect density, dielectric constant, electron affinity, bandgap, conduction and valence band effective density of states, ETL and HTL thicknesses, and both bulk and interfacial defect densities. The optimized device achieved a PCE of 26.69%, with VOC = 1.1127 V, JSC = 30.3156 mA/cm², and FF = 79.13%. The optimal absorber thickness was found to be 700 nm, the bandgap 1.4 eV, and the interfacial defect density 1×10¹4 cm⁻² at both interfaces. These results surpass recently reported simulation-based RbGeI₃ solar cells and are competitive with other high-performance lead-free perovskite devices. The findings demonstrate that the FTO/TiO₂/RbGeI₃/CuI/Au structure is a promising candidate for environmentally responsible next-generation photovoltaics.

# Introduction

## Background

The global demand for electrical energy has increased significantly over the past few decades owing to rapid population growth, industrialization, urbanization, and continuous technological advancement [1]. At present, most of the world's electricity is still generated from conventional fossil fuels, including coal, natural gas, and petroleum [2]. Although these energy resources have played a crucial role in economic development, their excessive utilization has accelerated greenhouse gas emissions, global warming, and environmental pollution [2]. Moreover, the continuous depletion of fossil fuel reserves has raised serious concerns regarding future energy security, emphasizing the need for sustainable and environmentally friendly energy alternatives [3].

Among various renewable energy resources, solar energy has attracted considerable attention because of its abundance, clean nature, and widespread availability [3]. Unlike fossil fuel-based power generation, photovoltaic (PV) systems convert solar radiation directly into electricity without producing harmful emissions during operation [4]. Continuous improvements in photovoltaic technology, together with decreasing manufacturing costs, have made solar energy one of the fastest-growing renewable energy sources worldwide [4].

Based on the absorber materials and fabrication technology, photovoltaic devices are generally classified into three generations. The first generation mainly consists of crystalline silicon solar cells, which dominate the commercial market because of their high efficiency and long-term operational stability. The second generation includes thin-film technologies such as cadmium telluride (CdTe), copper indium gallium selenide (CIGS), and amorphous silicon (a-Si), which require less semiconductor material and offer lower manufacturing costs. The third generation comprises emerging photovoltaic technologies, including dye-sensitized solar cells, organic solar cells, quantum-dot solar cells, and perovskite solar cells (PSCs), which aim to achieve high efficiency with low-cost fabrication processes [5].

Among these third-generation technologies, perovskite solar cells have emerged as one of the most rapidly developing photovoltaic technologies because of their remarkable optoelectronic properties and continuously improving power conversion efficiency [6]. Perovskite absorber materials possess the general chemical formula ABX₃, where A is a monovalent cation, B is a divalent metal cation, and X represents a halide anion [7]. These materials exhibit several attractive characteristics, including high optical absorption coefficients, tunable direct bandgaps, long carrier diffusion lengths, low exciton binding energies, and balanced electron and hole transport properties, making them highly suitable for photovoltaic applications [6].

Despite these advantages, the highest-performing perovskite solar cells reported to date are predominantly based on lead-containing absorber materials, such as methylammonium lead iodide (MAPbI₃) and formamidinium lead iodide (FAPbI₃) [8]. The presence of lead raises significant environmental and health concerns because lead compounds are toxic and may contaminate the environment during device fabrication, operation, or disposal [9]. Consequently, replacing lead with environmentally benign elements has become one of the primary research directions in perovskite photovoltaic technology [9].

Despite the rapid development of lead-based perovskite solar cells, their commercialization is still limited by the toxicity of lead and its potential environmental impact [10]. Therefore, considerable research has focused on developing lead-free perovskite materials by replacing lead with environmentally friendly elements such as tin (Sn), germanium (Ge), bismuth (Bi), and antimony (Sb) [11].

Tin-based perovskites have shown promising photovoltaic properties; however, the oxidation of Sn²⁺ to Sn⁴⁺ results in high defect densities and poor device stability [11], [12]. As an alternative, germanium-based perovskites have attracted increasing attention because of their suitable optoelectronic properties and improved environmental compatibility [12]. Among them, RbGeI₃ is considered a promising absorber material owing to its suitable bandgap, high optical absorption coefficient, and good thermal stability [13].

The performance of RbGeI₃-based perovskite solar cells is strongly influenced by the selection of appropriate charge transport layers and the optimization of key device parameters, such as absorber thickness, defect density, bandgap, electron affinity, and interface properties [12]. Since experimental optimization is both time-consuming and expensive, numerical simulation has become an effective approach for predicting device performance before fabrication [13]. Among the available simulation tools, SCAPS-1D is widely used because it accurately models charge transport and recombination mechanisms in multilayer solar cells.

Based on these considerations, this study investigates and optimizes a lead-free FTO/TiO₂/RbGeI₃/CuI/Au perovskite solar cell using the SCAPS-1D simulation software. Different ETL and HTL combinations are first evaluated to identify the best device configuration, followed by systematic optimization of the major material and device parameters to improve the photovoltaic performance of the proposed solar cell. To better understand the current progress and identify the existing research gap in lead-free RbGeI₃-based perovskite solar cells, a review of recent related studies is presented in the following section.

## Literature Review

The reviewed studies given in Table 1.1 Summary of literature review demonstrate that SCAPS-1D has become one of the most widely used numerical simulation tools for designing and optimizing lead-free perovskite solar cells before experimental fabrication. Previous researchers have investigated various lead-free absorber materials, including MASnI₃, CsSnI₃, CsGeI₃, and RbGeI₃, to overcome the toxicity associated with lead-based perovskites while maintaining satisfactory photovoltaic performance [20]–[22].

Most studies focused on optimizing important device parameters such as absorber thickness, doping concentration, defect density, interface defects, and operating temperature to improve the power conversion efficiency (PCE) [20], [21]. In addition, different electron transport layers (ETLs), including TiO₂, ZnO, SnO₂, and PCBM, as well as hole transport layers (HTLs) such as CuI, NiO, Spiro-OMeTAD, and CuSCN, have been investigated to improve charge extraction and suppress carrier recombination [22], [23]. Recent studies have also explored comprehensive optimization strategies by combining transport layer engineering with material parameter optimization to further enhance the performance of RbGeI₃-based perovskite solar cells [24], [25].

Table 1.1 Summary of literature review

| Work | Materials | Key Findings | Limitations |
| --- | --- | --- | --- |
| Shamas Mushtaq et al. (2023) | ETL: SnO2 Absorber: MASnBr3 HTL: NiO | PCE = 34.52%, FF = 88.30%, Voc = 1.1214 V | Very high theoretical efficiency. Absorber different from Ge-based system. |
| B.K. Ravidas et al. (2023) [14] | ETL: TiO2 Absorber: CsSnI3 HTL: P3HT, PEDOT:PSS, Spiro-OMeTAD | Established link between DFT-calculated bandgap and device efficiency | Not focused on multi-HTL comparative analysis |
| Dibyajyoti Saikia et al. (2022) [15] | ETL: TiO2 Absorber: CsGeI3 HTL: CuI | Voc = 0.667 V Optimized PCE = 10.8% FF = 73.49% | Did not build large HTL× ETL comparative matrix |
| M. Khalid Hossain et al. (2023) [16] | ETL: TiO2 Absorber: CsPbI3 HTL: CBTS | Maximum PCE = 19.06% achieved after device optimization. Proper ETL/HTL selection improved charge transport and reduced recombination. Device performance strongly affected by defect density, interface traps, and absorber thickness. | Study focused only on lead-based CsPbI₃ perovskite. Limited comparison of ETL and HTL materials. Long-term stability and environmental effects not analyzed. |
| Sarra Bouazizi et al. (2022) [17] | ETL: PCBM Absorber: CsSnI3 HTL: CuI | Optimized ETL/HTL doping ≈10¹⁹ cm⁻³. Best thickness ≈480 nm. ZnO best ETL. Max PCE = 18.13%. | Very low defect density hard to realize. Efficiency drops at high temperature |
| Hossain et al. (2023) [18] | ETL: PCBM Absorber: CsSnI3 HTL: CuI | Direct bandgap CsSnI₃ (~0.95 eV) confirmed by DFT. Optimized structure ITO/PCBM/CsSnI₃/CuI/ Au achieved ≈10.1% PCE. Proper ETL/HTL band alignment improved charge transport. Lower ETL and absorber thickness enhanced device performance. High shunt resistance improved efficiency | Defect density fixed (10¹⁵ cm⁻³) → not realistic. PCE still moderate (~10–11%). |
| Grishma Pindolia et al. (2022) [13] | ETL: TiO2 Absorber: RbGeI3 HTL: NiO | NiO (HTL) and TiO₂ (ETL) showed best device performance. Optimized thickness: RbGeI₃ = 500 nm, NiO = 100 nm, TiO₂ = 50 nm. Optimal doping ≈ 10¹⁹ cm⁻³ improves charge transport. Achieved PCE = 10.11%, FF = 63.68%. | Efficiency still lower than lead-based PSCs. Device sensitive to defect density and temperature. |
| Advik Pathak et al. (2026) [19] | ETL: TiO2 Absorber: MAGeI₃, FAGeI₃, CsGeI₃, RbGeI₃ HTL: Spiro-OMeTAD | RbGeI₃ showed the best performance with PCE ≈ 26.47%. Optimal absorber thickness ≈ 400 nm. Higher carrier mobility and lower recombination improved efficiency. CsGeI₃ showed high Voc but lower current density. | Germanium perovskites suffer from Ge²⁺ oxidation to Ge⁴⁺, creating high defect density. High defect density increases recombination and reduces device stability and efficiency. |
| Nishad et al. (2025) [20] | Various Cu-based HTLs using RbGeI3 PSC | Investigated several Cu-based HTLs and demonstrated that proper HTL selection significantly improves carrier extraction and device efficiency | Focused mainly on HTL selection; comprehensive optimization of material parameters was not performed. |
| Chen et al. (2025) [21] | Gradient-doped RbGeI₃ perovskite solar cell | Proposed gradient doping in the RbGeI₃ absorber to enhance charge transport and improve photovoltaic performance. | Concentrated on doping profile optimization without evaluating multiple ETL–HTL combinations. |
| Dash et al. (2025) [22] | DFT + SCAPS study of RbGeCl₃, RbGeBr₃ and RbGeI₃ | Combined DFT calculations with SCAPS-1D simulation and reported RbGeI₃ as the most promising absorber among the RbGeX₃ family after device optimization. | Focused primarily on material comparison and theoretical optimization rather than comprehensive device architecture optimization. |

### Research Gap

Although significant progress has been achieved, most previous studies optimized only a limited number of device parameters or investigated a single device configuration [20]–[24]. A comprehensive optimization involving ETL–HTL selection together with absorber thickness, dielectric constant, bandgap, electron affinity, density of states (DOS), bulk defect density, and interface defect density has rarely been reported for a single RbGeI₃-based device [25].

Therefore, this study proposes a systematic SCAPS-1D optimization of an FTO/TiO₂/RbGeI₃/CuI/Au perovskite solar cell. Different ETL–HTL combinations are first compared to identify the optimum device structure, followed by comprehensive optimization of the major material and electrical parameters to achieve enhanced photovoltaic performance and provide useful guidelines for future experimental development.

## Thesis Objectives

The main objective of this research is to investigate and optimize the photovoltaic performance of a lead-free RbGeI₃ absorber-based perovskite solar cell using the SCAPS-1D simulation software. The study aims to identify an efficient and environmentally friendly device structure through systematic optimization of material and electrical parameters.

The specific objectives of this study are as follows:

- To design and simulate different RbGeI₃-based perovskite solar cell configurations using SCAPS-1D [23].

- To compare different electron transport layer (ETL) and hole transport layer (HTL) combinations in order to identify the optimum device architecture [13].

- To optimize important device parameters, including absorber thickness, ETL thickness, HTL thickness, dielectric constant, bandgap, electron affinity, defect density, interface defect density, and density of states (DOS), for improved photovoltaic performance [13].

- To analyze the effects of these parameters on the open-circuit voltage (VOC), short-circuit current density (JSC), fill factor (FF), and power conversion efficiency (PCE) [6].

- To compare the simulated results with previously reported studies and evaluate the effectiveness of the proposed device structure [13].

## Thesis Organization

This thesis is organized into four chapters. Chapter 1 introduces the research background, presents a review of the relevant literature, identifies the research gap, and outlines the objectives of the study. Chapter 2 describes the materials and methodology, including the SCAPS-1D simulation tool, device structure, material selection, simulation parameters, performance evaluation, and optimization procedures. Chapter 3 presents the simulation results and discusses the effects of various material and device parameters on the photovoltaic performance of the proposed lead-free RbGeI₃-based perovskite solar cell. Finally, Chapter 4 summarizes the major findings of the study, presents the overall conclusions, and provides recommendations for future research on lead-free perovskite solar cells.

# Theoretical background and working principle

## Research Methodology

This research adopted a numerical simulation approach to investigate and optimize the photovoltaic performance of a lead-free perovskite solar cell using the Solar Cell Capacitance Simulator in One Dimension (SCAPS-1D, version 3.3.10). Numerical simulation has become an important research tool in photovoltaic engineering because it enables researchers to investigate the influence of different material properties and device parameters before experimental fabrication. This approach significantly reduces the cost and time required for device development while providing a better understanding of the physical mechanisms governing solar cell operation [24].

The proposed solar cell consists of a conventional FTO/TiO₂/RbGeI₃/CuI/Au device architecture, where fluorine-doped tin oxide (FTO) acts as the transparent conducting oxide (TCO), titanium dioxide (TiO₂) serves as the electron transport layer (ETL), rubidium germanium iodide (RbGeI₃) functions as the absorber layer, copper iodide (CuI) is employed as the hole transport layer (HTL), and gold (Au) is used as the back metal contact. This configuration was selected because the constituent materials exhibit suitable energy band alignment, good carrier transport capability, and eliminate the environmental concerns associated with lead-based perovskite solar cells [2,18] .

The material parameters required for the simulation, including bandgap energy, electron affinity, dielectric constant, carrier mobility, effective density of states, doping concentration, and defect density, were collected from previously published experimental and numerical studies on lead-free perovskite solar cells [2,18,23]. These parameters were carefully incorporated into the SCAPS-1D simulator to establish a realistic baseline device before performing further optimization.

After constructing the initial device, a systematic optimization procedure was carried out by varying one parameter at a time while keeping all remaining parameters constant. This approach makes it possible to evaluate the individual influence of each parameter on the photovoltaic performance without interference from other variables. The optimized value obtained from each simulation step was then used as the input for the subsequent optimization process. Such a sequential optimization strategy is widely adopted in SCAPS-based photovoltaic studies because it provides a clear understanding of the contribution of each device parameter to the overall solar cell performance [18] [25].

The optimization process included the investigation of absorber layer thickness, absorber defect density, dielectric constant, electron affinity, absorber bandgap, conduction and valence band effective density of states, ETL thickness, HTL thickness, and both bulk and interface defect densities. In addition, the quantum efficiency (QE) spectrum and equilibrium energy band diagram were analyzed to investigate the optical response, carrier collection efficiency, and charge transport behavior of the optimized device.

All simulations were performed under the standard AM 1.5G solar spectrum with an incident illumination intensity of 100 mW/cm² at an operating temperature of 300 K. The current density–voltage (J–V) characteristics were calculated under illuminated conditions to obtain the open-circuit voltage (VOC), short-circuit current density (JSC), fill factor (FF), and power conversion efficiency (PCE). These four parameters were used to evaluate the overall performance of the proposed lead-free perovskite solar cell [26].

Finally, the optimized photovoltaic parameters obtained from the present study were compared with previously reported experimental and numerical investigations on RbGeI₃- and other lead-free Ge/Sn-based perovskite solar cells. This comparison was carried out to evaluate the reliability of the proposed device architecture and to identify the remaining challenges for future experimental realization [2,18].

## SCAPS-1D Simulation Tool

The photovoltaic performance of the proposed lead-free perovskite solar cell was investigated using the Solar Cell Capacitance Simulator in One Dimension (SCAPS-1D), version 3.3.10. SCAPS-1D is a one-dimensional numerical simulation software developed by the Department of Electronics and Information Systems (ELIS), Ghent University, Belgium, for modelling and analyzing thin-film photovoltaic devices [22].

SCAPS-1D has become one of the most widely used simulation tools in photovoltaic research because it provides a simple and reliable platform for studying the electrical characteristics of different types of solar cells, including CdTe, CIGS, CZTS, organic, and perovskite solar cells [22,23]. Unlike experimental fabrication, numerical simulation enables researchers to investigate the influence of different material properties and device parameters individually, making it possible to optimize the device structure before practical implementation [18].

The simulator solves the fundamental semiconductor transport equations self-consistently throughout the device structure. These equations include the Poisson equation, the electron continuity equation, and the hole continuity equation, which describe the electrostatic potential, carrier generation, carrier transport, and recombination mechanisms inside the solar cell [22]. By solving these coupled equations simultaneously, SCAPS-1D predicts the electrical behavior of the device under both dark and illuminated operating conditions.

The Poisson equation determines the electrostatic potential distribution inside the device and is expressed as:

∇·ε∇ψ=-qp-n+ND+-NA-+ρt

where ε is the dielectric permittivity, ψ is the electrostatic potential, q is the elementary charge, n and p represent the electron and hole concentrations, N_D and N_A denote the donor and acceptor concentrations, respectively, and ρ_t represents the trapped charge density [22].

The transport of electrons inside the device is governed by the electron continuity equation,

1/qdJn/dx=G-R

where Jₙ is the electron current density, G is the carrier generation rate, and R is the carrier recombination rate [22].

Similarly, the hole transport is described by the hole continuity equation,

-1/qdJp/dx=G-R

where Jₚ is the hole current density. Together, these equations describe the generation, transport, and recombination of charge carriers throughout the solar cell under illumination [22].

SCAPS-1D allows users to define the physical properties of each semiconductor layer individually. These parameters include layer thickness, bandgap energy, electron affinity, dielectric constant, effective density of states, carrier mobility, donor concentration, acceptor concentration, defect density, interface defect density, and contact work function. The software then calculates the resulting electrical characteristics based on these input parameters [23].

In the present work, SCAPS-1D version 3.3.10 was employed to simulate the FTO/TiO₂/RbGeI₃/CuI/Au device structure under the standard AM 1.5G solar spectrum with an incident power density of 100 mW cm⁻² at a temperature of 300 K. The simulator was used to evaluate the current density–voltage (J–V) characteristics, quantum efficiency (QE), energy band alignment, and photovoltaic parameters of the proposed device. Furthermore, systematic optimization was carried out by varying different material and interface parameters while maintaining the remaining parameters constant. This procedure enabled the identification of the optimum device configuration with improved photovoltaic performance.

Figure 2.1 Graphical user interface of SCAPS-1D (Version 3.3.10) used for device simulation.

## Device Structure and Working Principle

The proposed lead-free perovskite solar cell investigated in this work consists of a conventional n-i-p planar heterojunction architecture with the configuration:

FTO/TiO₂/RbGeI₃/CuI/Au

This device architecture was selected because it provides efficient charge separation, rapid carrier transport, and suitable energy level alignment while eliminating the environmental and health concerns associated with lead-based perovskite absorbers [2,18].

Figure 2.2 Schematic diagram of the proposed FTO/TiO₂/RbGeI₃/CuI/Au perovskite solar cell structure.

Front Electrode: FTO

ETL: TiO2

Absorber: RbGeI3

HTL: CuI

Back Electrode: Au

Sunlight

The complete device consists of five functional layers: a transparent conducting oxide (FTO), an electron transport layer (TiO₂), a lead-free perovskite absorber (RbGeI₃), a hole transport layer (CuI), and a gold (Au) back contact. The layer sequence employed in this study is illustrated schematically in Figure 2.2.

### Transparent Conducting Oxide (FTO)

Fluorine-doped tin oxide (FTO) serves as the front transparent conducting electrode of the solar cell. It possesses high optical transparency in the visible spectrum together with excellent electrical conductivity, allowing incident sunlight to reach the absorber layer while simultaneously collecting the generated electrons with minimal resistive loss [24]. In the present work, the thickness of the FTO layer was fixed at 500 nm, consistent with values commonly reported for perovskite solar cells.

### Electron Transport Layer (TiO₂)

Titanium dioxide (TiO₂) was employed as the electron transport layer (ETL). The primary function of the ETL is to extract photogenerated electrons from the absorber layer and transport them toward the FTO electrode while effectively blocking holes. Due to its wide bandgap, favorable conduction band position, good chemical stability, and low fabrication cost, TiO₂ has become one of the most widely used ETL materials in perovskite solar cells [27].

Based on the optimization performed in this work, the TiO₂ layer thickness was fixed at 10 nm.

### Absorber Layer (RbGeI₃)

The RbGeI₃ perovskite layer functions as the photoactive absorber where incident photons are absorbed to generate electron–hole pairs. Compared with conventional lead-based perovskites, RbGeI₃ offers the important advantage of being environmentally friendly because germanium replaces toxic lead while maintaining desirable optoelectronic properties.

The absorber thickness used in the optimized device was 700 nm, which provides sufficient optical absorption while maintaining efficient carrier transport and minimizing bulk recombination losses. The optimized material parameters adopted in this work include:

- Bandgap = 1.31 eV

- Electron affinity = 3.9 eV

- Relative dielectric constant = 15

- Electron mobility = 28.6 cm² V⁻¹ s⁻¹

- Hole mobility = 27.3 cm² V⁻¹ s⁻¹

These values were selected based on literature reports and subsequent optimization using SCAPS-1D.

### Hole Transport Layer (CuI)

Copper iodide (CuI) was selected as the hole transport layer owing to its excellent hole conductivity, high optical transparency, appropriate valence band alignment, and comparatively low fabrication cost [27]. The HTL facilitates efficient extraction of photogenerated holes from the absorber layer while preventing electron back transfer toward the rear electrode.

The optimized CuI thickness employed in this work was 100 nm.

### Back Metal Contact (Au)

Gold (Au) was used as the rear metal contact because of its high work function, excellent electrical conductivity, and superior chemical stability. A high-work-function metal establishes an ohmic contact with the hole transport layer, thereby reducing contact resistance and improving hole collection efficiency [27].

### Working Principle of the Proposed Solar Cell

When sunlight is incident on the front surface of the device, photons first pass through the transparent FTO electrode and TiO₂ layer before reaching the RbGeI₃ absorber. Photons with energies greater than the absorber bandgap are absorbed within the RbGeI₃ layer, generating electron–hole pairs.

The built-in electric field established across the heterojunction separates these photogenerated carriers. Electrons are transported from the absorber into the TiO₂ electron transport layer and subsequently collected by the FTO electrode. Simultaneously, holes move toward the CuI hole transport layer before being collected by the Au back contact. This directional carrier transport minimizes carrier recombination and contributes to improved photovoltaic performance [27].

The optimized device architecture investigated in this study was subsequently analyzed using SCAPS-1D to evaluate the current density–voltage characteristics, quantum efficiency, energy band alignment, and charge transport behavior under standard AM 1.5G illumination.

# Chapter 3: Material selection and parameters

## Material selection

### Selection of Electron Transport Layer (TiO₂)

The electron transport layer (ETL) is an indispensable component of a perovskite solar cell because it governs the extraction and transport of photogenerated electrons from the absorber layer to the front electrode while simultaneously blocking holes from flowing in the opposite direction. Efficient charge separation at the ETL/perovskite interface minimizes carrier recombination and directly influences the open-circuit voltage (VOC), fill factor (FF), and overall power conversion efficiency (PCE) of the device [28], [29]. Consequently, selecting an appropriate ETL is essential for achieving high photovoltaic performance and long-term operational stability.

An ideal electron transport material should possess several important characteristics. These include high electron mobility, excellent optical transparency, suitable conduction band alignment with the absorber layer, low density of defect states, good chemical compatibility, and high thermal stability [30]. In addition, the ETL should form a uniform and compact interface with the perovskite absorber to suppress trap-assisted recombination and facilitate efficient carrier extraction. Poor interfacial contact or unfavorable energy band alignment can significantly increase recombination losses, thereby reducing the overall device efficiency [29].

Among the various electron transport materials investigated for perovskite solar cells, such as ZnO, SnO₂, CdS, WO₃, PCBM and TiO₂, titanium dioxide (TiO₂) has remained one of the most extensively studied and successfully employed inorganic ETLs. This widespread use is primarily attributed to its balanced combination of electrical, optical and chemical properties, together with its excellent compatibility with different perovskite absorber materials [30], [31].

TiO₂ is an n-type semiconductor with a wide bandgap of approximately 3.2 eV in its anatase phase. Because of this wide bandgap, the material exhibits excellent transparency throughout the visible region of the solar spectrum, allowing most incident photons to reach the RbGeI₃ absorber layer with negligible parasitic absorption [30]. As a result, the majority of photon absorption occurs inside the perovskite layer, where electron-hole pairs are generated efficiently. Maintaining high optical transparency in the ETL is particularly important because any unnecessary absorption before light reaches the absorber directly limits the photocurrent generation.

Besides its optical properties, TiO₂ possesses favorable energy band alignment with halide perovskite absorbers. The conduction band minimum of TiO₂ lies slightly below that of most iodide-based perovskites, providing an energetically favorable pathway for photogenerated electrons to transfer from the absorber into the ETL [29]. At the same time, its deep valence band acts as an effective barrier against hole transport, thereby suppressing interfacial recombination. Recent spectroscopic investigations have demonstrated that appropriate band alignment between TiO₂ and the perovskite absorber accelerates electron extraction kinetics and enhances charge separation, ultimately contributing to improved photovoltaic performance [29].

The electrical characteristics of TiO₂ also make it a suitable electron transport material. Although its intrinsic electron mobility is lower than that of ZnO and SnO₂, TiO₂ provides sufficiently fast electron transport when fabricated with appropriate morphology and crystallinity [5]. More importantly, TiO₂ forms chemically stable interfaces with perovskite materials and exhibits relatively low interfacial defect density after suitable surface treatment. Reducing interface defects is essential because these defects act as non-radiative recombination centers that shorten carrier lifetime and decrease device efficiency [32].

Another significant advantage of TiO₂ is its outstanding chemical and thermal stability. Unlike several alternative ETLs, TiO₂ is resistant to moisture, ultraviolet radiation, and chemical degradation under normal operating conditions [30]. It is also environmentally benign, inexpensive, and can be deposited using a variety of well-established techniques, including spin coating, spray pyrolysis, chemical bath deposition, sputtering, atomic layer deposition, and sol-gel processing. These versatile fabrication routes enable precise control over film thickness, crystallinity, and surface morphology while remaining compatible with large-scale manufacturing processes [28].

Although alternative electron transport materials such as ZnO and SnO₂ have recently attracted considerable attention because of their higher electron mobility and low-temperature processing capability, each presents certain limitations. ZnO may chemically react with iodide-based perovskite absorbers, accelerating device degradation, whereas SnO₂ often requires careful surface modification to minimize interface defects and optimize energy level alignment [30]. Consequently, TiO₂ continues to serve as a reliable benchmark ETL in both experimental and simulation-based investigations owing to its excellent reproducibility, stable interface formation, and well-understood physical properties.

The present work employs a planar FTO/TiO₂/RbGeI₃/CuI/Au device architecture. In this configuration, TiO₂ provides an effective pathway for transporting photogenerated electrons from the RbGeI₃ absorber to the fluorine-doped tin oxide (FTO) electrode while preventing the back transfer of holes. Its favorable conduction band alignment with RbGeI₃, combined with high optical transparency and excellent chemical stability, makes it highly suitable for lead-free germanium-based perovskite solar cells. Furthermore, numerous experimental and theoretical studies have demonstrated that TiO₂-based devices exhibit stable operation, reduced recombination losses, and enhanced charge extraction efficiency when the interface quality is carefully optimized [29]. Considering these advantages, TiO₂ was selected as the electron transport layer for the proposed device in the present study.

### Selection of Absorber Layer (RbGeI3)

The absorber layer is the core component of a perovskite solar cell (PSC) because it is responsible for absorbing incident solar radiation and generating electron–hole pairs. Therefore, the overall photovoltaic performance of a PSC largely depends on the optical and electrical properties of the absorber material. An ideal absorber should possess a suitable direct bandgap, high optical absorption coefficient, long carrier diffusion length, low defect density, and excellent charge transport characteristics to maximize the conversion of sunlight into electrical energy [33].

Conventional PSCs mainly employ lead-based perovskites such as MAPbI₃ and FAPbI₃ owing to their excellent optoelectronic properties and high power conversion efficiencies. However, the toxicity of lead and the potential environmental risks associated with its large-scale application have become major obstacles to commercial deployment. As a result, considerable research efforts have been devoted to developing environmentally friendly lead-free perovskite materials without significantly compromising device performance [33], [34].

Among the various lead-free alternatives, germanium (Ge)-based inorganic perovskites have attracted increasing attention because germanium belongs to the same group as lead in the periodic table and exhibits similar electronic configurations. Consequently, Ge-based perovskites can retain many desirable electronic properties of Pb-based materials while eliminating the toxicity associated with lead. Moreover, all-inorganic germanium perovskites generally exhibit better thermal stability than hybrid organic-inorganic perovskites, making them attractive candidates for long-term photovoltaic applications [34], [35].

Rubidium germanium iodide (RbGeI₃) is one of the most promising lead-free inorganic perovskite absorbers investigated in recent years. It crystallizes in the ABX₃ perovskite structure, where rubidium (Rb) occupies the A-site, germanium (Ge) occupies the B-site, and iodine (I) forms the halide framework. This crystal structure provides excellent structural stability and enables efficient light absorption over a broad region of the solar spectrum [35], [36].

One of the major advantages of RbGeI₃ is its suitable direct bandgap, which lies in the range of approximately 1.30–1.40 eV, depending on crystal structure and computational method [4], [6]. This bandgap is close to the optimum value predicted by the Shockley–Queisser limit for single-junction solar cells. Consequently, RbGeI₃ can effectively absorb visible light while maintaining a sufficiently high open-circuit voltage, making it an attractive absorber for high-efficiency photovoltaic devices [37].

Besides its favorable bandgap, RbGeI₃ possesses a high optical absorption coefficient, allowing a large fraction of incident photons to be absorbed within a relatively thin absorber layer [36], [37]. This characteristic reduces the required absorber thickness while maintaining efficient photogeneration of charge carriers. Furthermore, first-principles studies have reported that RbGeI₃ exhibits suitable dielectric properties, low effective carrier masses, and good carrier transport characteristics, all of which contribute to efficient charge separation and reduced recombination losses.

Compared with tin-based lead-free perovskites such as MASnI₃ or FASnI₃, RbGeI₃ offers an additional advantage in terms of chemical stability. Tin-based absorbers often suffer from the oxidation of Sn²⁺ to Sn⁴⁺, which introduces deep defect states and accelerates device degradation under ambient conditions [3]. In contrast, germanium-based perovskites have demonstrated comparatively improved structural stability and have therefore emerged as promising candidates for developing durable lead-free PSCs [33]. Although germanium may also undergo oxidation under certain conditions, recent studies have shown that appropriate interface engineering and device optimization can effectively improve the stability and photovoltaic performance of RbGeI₃-based solar cells.

Recent theoretical investigations based on density functional theory (DFT) have further confirmed that RbGeI₃ possesses favorable electronic and optical properties for photovoltaic applications. The calculated electronic band structure reveals a direct bandgap with strong optical absorption throughout the visible region, while density of states analysis indicates efficient electronic transitions near the band edges. These properties facilitate effective photon absorption and rapid generation of free charge carriers, which are essential for achieving high photovoltaic efficiency [38].

In the present work, RbGeI₃ was selected as the absorber layer because its optoelectronic properties are well matched with the selected TiO₂ electron transport layer and CuI hole transport layer. The favorable band alignment among these layers promotes efficient charge separation and carrier transport while suppressing interfacial recombination. Moreover, the lead-free nature, suitable bandgap, excellent optical absorption, and promising stability of RbGeI₃ make it an appropriate absorber material for developing environmentally friendly and high-performance perovskite solar cells. Therefore, the FTO/TiO₂/RbGeI₃/CuI/Au device architecture was adopted in this study to investigate and optimize the photovoltaic performance of lead-free perovskite solar cells.

### Selection of Hole Transport Layer (CuI)

The hole transport layer (HTL) plays a vital role in the operation of a perovskite solar cell by extracting photogenerated holes from the absorber layer and transporting them efficiently to the back metal electrode. Simultaneously, it blocks the transport of electrons, thereby minimizing charge recombination at the absorber/back-contact interface. Consequently, the selection of a suitable HTL has a direct influence on the open-circuit voltage (VOC), fill factor (FF), and overall power conversion efficiency (PCE) of the device [39].

An ideal hole transport material should possess high hole mobility, suitable valence band alignment with the absorber layer, excellent optical transparency, low defect density, and good chemical stability. In addition, it should form a stable interface with the perovskite absorber to facilitate rapid hole extraction while suppressing non-radiative recombination losses [39], [40].

Several organic and inorganic materials have been investigated as HTLs in perovskite solar cells, including Spiro-OMeTAD, PEDOT:PSS, NiO, CuSCN, Cu₂O and CuI. Although organic HTLs such as Spiro-OMeTAD have enabled high device efficiencies, they generally require expensive dopants and additives, exhibit relatively low thermal stability, and are sensitive to moisture. These drawbacks increase fabrication cost and limit the long-term stability of perovskite solar cells [41], [42].

In contrast, copper iodide (CuI) has emerged as a promising inorganic HTL because it combines good electrical properties with excellent chemical stability. CuI is a p-type semiconductor with a wide bandgap of approximately 3.1 eV, ensuring high transparency in the visible region so that very little incident light is absorbed by the HTL before reaching the perovskite absorber [43], [44]. In addition, CuI possesses high hole conductivity and favorable valence band alignment with many iodide-based perovskites, enabling efficient hole extraction while effectively blocking electrons at the HTL/absorber interface [3], [6].

Another important advantage of CuI is its excellent carrier transport capability. The relatively high hole mobility of CuI reduces series resistance within the device and facilitates rapid charge collection at the back contact. Efficient hole extraction minimizes carrier accumulation at the interface, thereby reducing recombination losses and improving both the fill factor and overall device efficiency [43], [45]. Furthermore, CuI forms compact and chemically stable interfaces with inorganic perovskite absorbers, which contributes to improved operational stability under prolonged illumination and elevated temperatures.

Compared with other inorganic HTLs such as NiO and CuSCN, CuI offers several practical advantages. CuSCN exhibits suitable energy level alignment but often suffers from solvent compatibility issues during device fabrication. NiO provides excellent stability; however, intrinsic defects and surface traps may introduce additional recombination centers if the interface is not properly engineered. CuI provides a balanced combination of suitable energy band alignment, high hole conductivity, simple fabrication, and low processing cost, making it an attractive HTL for both experimental fabrication and numerical simulation of perovskite solar cells [39], [42].

Recent experimental studies have demonstrated that replacing conventional organic HTLs with CuI can improve device stability while maintaining competitive photovoltaic performance. Because CuI is an inorganic, earth-abundant, and low-cost material, it is considered a promising alternative for developing stable and environmentally friendly perovskite solar cells. Its compatibility with lead-free perovskite absorbers has also attracted considerable attention in recent years, particularly for all-inorganic device architectures .

In the present work, CuI was selected as the hole transport layer for the FTO/TiO₂/RbGeI₃/CuI/Au solar cell owing to its favorable valence band alignment with the RbGeI₃ absorber, high hole mobility, excellent optical transparency, and superior chemical stability. These characteristics promote efficient hole extraction while suppressing interfacial recombination, thereby contributing to enhanced photovoltaic performance. Moreover, the use of an inorganic HTL is consistent with the objective of developing a stable and lead-free perovskite solar cell architecture suitable for long-term photovoltaic applications.

### Selection of Front Contact (FTO)

The front contact is one of the essential components of a perovskite solar cell because it acts as the transparent conducting electrode through which sunlight enters the device while simultaneously collecting and transporting the photogenerated electrons to the external circuit. Therefore, an ideal front contact should possess high optical transparency, low electrical resistance, good thermal stability, and excellent chemical compatibility with the electron transport layer (ETL) .

Transparent conducting oxides (TCOs) are commonly employed as front electrodes in perovskite solar cells. Among the available TCO materials, indium tin oxide (ITO) and fluorine-doped tin oxide (FTO) are the most widely used because they exhibit high electrical conductivity together with excellent transparency in the visible region [46]. However, for regular n-i-p planar perovskite solar cells, FTO has become the preferred substrate due to its superior thermal stability and chemical durability during device fabrication [47].

Fluorine-doped tin oxide (FTO) is an n-type semiconductor prepared by introducing fluorine atoms into the SnO₂ crystal lattice. The incorporation of fluorine increases the free electron concentration, resulting in low sheet resistance while maintaining high optical transmittance in the visible wavelength region [48], [49]. As a result, FTO can efficiently transmit incident sunlight to the absorber layer while simultaneously providing an effective pathway for collecting photogenerated electrons.

Another important advantage of FTO is its excellent thermal and chemical stability. Unlike ITO, whose electrical properties may deteriorate during high-temperature processing, FTO remains stable even at temperatures above 450°C. This characteristic makes it highly compatible with TiO₂-based electron transport layers, which are commonly fabricated or annealed at elevated temperatures to improve crystallinity and electron transport properties [47], [50]. Consequently, FTO has become the standard transparent electrode in many experimental and simulation studies involving TiO₂-based perovskite solar cells.

The surface morphology of FTO also contributes to device performance. Commercial FTO-coated glass generally exhibits a rough surface texture that enhances light scattering within the solar cell, increasing the optical path length inside the absorber layer. This light-trapping effect improves photon absorption and can contribute to a higher short-circuit current density (JSC) [48]. Furthermore, the good electrical contact between FTO and TiO₂ facilitates efficient electron extraction while minimizing contact resistance.

Although ITO generally exhibits slightly higher electrical conductivity than FTO, it contains indium, which is relatively expensive and less abundant. Moreover, ITO is more susceptible to degradation during high-temperature processing and under certain chemical environments encountered during perovskite device fabrication [47]. In contrast, FTO offers excellent mechanical robustness, lower fabrication cost, and better long-term stability, making it a more practical choice for regular n-i-p perovskite solar cells.

In the present study, FTO was selected as the front contact for the FTO/TiO₂/RbGeI₃/CuI/Au device architecture because of its high optical transparency, low sheet resistance, excellent thermal stability, and strong compatibility with the TiO₂ electron transport layer. These characteristics facilitate efficient light transmission, rapid electron collection, and stable device operation, thereby supporting the overall objective of developing a high-performance and lead-free perovskite solar cell.

### Selection of Back Contact (Au)

The back metal contact serves as the final charge-collecting electrode in a perovskite solar cell. After photogenerated holes are transported through the hole transport layer (HTL), they are collected by the back electrode and delivered to the external circuit. Therefore, the electrical properties of the back contact significantly influence charge extraction, contact resistance, and overall device performance. An ideal back electrode should possess high electrical conductivity, an appropriate work function, excellent chemical stability, and good compatibility with the hole transport layer [44], [51].

Several metals, including aluminum (Al), silver (Ag), copper (Cu), nickel (Ni), platinum (Pt), and gold (Au), have been investigated as back contact materials for perovskite solar cells. The selection of the back electrode primarily depends on its work function and its ability to form an ohmic contact with the HTL. A suitable work function minimizes the energy barrier for hole extraction, thereby reducing contact resistance and improving charge collection efficiency [51], [52].

Among these materials, gold (Au) has become one of the most widely used back electrodes in high-performance perovskite solar cells because of its high work function (approximately 5.1 eV), excellent electrical conductivity, and superior chemical stability [44]. The high work function of Au closely matches the valence band of commonly used hole transport materials such as CuI, Spiro-OMeTAD, and NiO, allowing efficient hole extraction while suppressing electron leakage toward the back contact. This favorable energy level alignment contributes to a higher built-in potential, reduced carrier recombination, and improved open-circuit voltage (VOC) [52], [53].

Another important advantage of gold is its excellent resistance to oxidation and corrosion. Unlike aluminum and copper, which readily oxidize under ambient conditions, Au remains chemically stable during device fabrication and long-term operation. This stability helps preserve the electrical characteristics of the metal/HTL interface and contributes to the long-term reliability of the solar cell [44], [54]. Moreover, Au can be easily deposited by thermal evaporation, producing a dense and uniform electrode with low contact resistance.

Although silver exhibits excellent electrical conductivity and lower material cost than gold, it can react with iodide ions originating from the perovskite layer, leading to the formation of silver iodide (AgI) and gradual device degradation [54]. Similarly, aluminum possesses a relatively low work function, which may create a larger energy barrier for hole extraction and reduce device efficiency [52]. Platinum offers an even higher work function than Au but is significantly more expensive, making it less attractive for practical photovoltaic applications [51]. Consequently, Au provides a well-balanced combination of electrical performance, chemical stability, and device reliability.

Numerical simulation studies have also demonstrated that increasing the work function of the back contact generally improves the built-in electric field, facilitating efficient hole collection and reducing recombination losses near the HTL/metal interface [3]. In many SCAPS-1D simulations, Au consistently provides higher values of VOC, fill factor (FF), and power conversion efficiency (PCE) than lower work-function metals, making it a common choice for optimizing perovskite solar cell performance [52].

In the present study, Au was selected as the back contact for the FTO/TiO₂/RbGeI₃/CuI/Au device architecture because its high work function forms an efficient ohmic contact with the CuI hole transport layer, enabling rapid hole extraction with minimal energy loss. In addition, its excellent electrical conductivity, chemical inertness, and compatibility with the selected device structure contribute to stable and efficient photovoltaic operation. Therefore, Au is considered the most suitable back electrode for evaluating the photovoltaic performance of the proposed lead-free RbGeI3-based perovskite solar cell.

Table 3.1 Justification for the Selection of Materials Used in the Proposed Perovskite Solar Cell

| Device Layer | Selected Material | Primary Function | Reason for Selection |
| --- | --- | --- | --- |
| Front Contact | FTO | Transparent conducting electrode | High optical transparency, low sheet resistance, excellent thermal and chemical stability, and good compatibility with TiO₂ ETL. |
| Electron Transport Layer (ETL) | TiO₂ | Electron extraction and transport | Suitable band alignment with RbGeI₃, high transparency, chemical stability, and low interfacial recombination. |
| Absorber Layer | RbGeI₃ | Light absorption and charge generation | Lead-free composition, direct bandgap (~1.3–1.4 eV), strong optical absorption, and favorable optoelectronic properties. |
| Hole Transport Layer (HTL) | CuI | Hole extraction and transport | High hole mobility, wide bandgap, favorable valence band alignment, and excellent chemical stability. |
| Back Contact | Au | Hole collection electrode | High work function, excellent electrical conductivity, chemical inertness, and efficient ohmic contact with CuI. |

## Material Parameters

The accuracy of numerical simulation using SCAPS-1D strongly depends on the selection of appropriate material parameters for each layer of the solar cell. These parameters determine the electrical and optical behavior of the device and directly influence the simulated photovoltaic characteristics. Therefore, the material parameters used in this study were carefully selected from previously published experimental and theoretical investigations to ensure that the simulation closely represents the practical behavior of lead-free perovskite solar cells [55].

The proposed device consists of five functional layers: fluorine-doped tin oxide (FTO) as the transparent conducting oxide, TiO₂ as the electron transport layer (ETL), RbGeI₃ as the perovskite absorber layer, CuI as the hole transport layer (HTL), and Au as the back metal contact. Each material is characterized by several important physical parameters, including thickness, bandgap, electron affinity, dielectric permittivity, carrier mobility, effective density of states, doping concentration, and defect density. These parameters collectively govern charge generation, carrier transport, recombination, and charge collection within the device [55].

Most of the initial material parameters employed in this work were adopted from previously reported literature on RbGeI₃-based and other lead-free perovskite solar cells. However, several parameters, such as absorber thickness, transport layer thickness, defect density, electron affinity, and dielectric constant, were further optimized during the simulation process to achieve improved photovoltaic performance. The optimized values and their effects on the device characteristics are discussed in detail in Section 3.9.

The electrical and optical parameters used as the initial input values for the SCAPS-1D simulation are summarized in  Table 3.2, while the interface defect parameters employed at the ETL/absorber and absorber/HTL interfaces are presented in Table 3.3.

Table 3.2 Initial Electrical and Optical Parameters Used in the SCAPS-1D Simulation of the Proposed FTO/TiO₂/RbGeI₃/CuI/Au Solar Cell

| Parameters | TiO2 [14] | FTO [13] | RbGeI3 [13] | CuI [18] |
| --- | --- | --- | --- | --- |
| Thickness (nm) | 30 | 500 | 400 | 100 |
| Bandgap Eg (eV) | 3.2 | 3.2 | 1.31 | 3.1 |
| Affinity χ (eV) | 4 | 4.4 | 3.9 | 2.1 |
| Dielectric Permittivity (∊r) | 9 | 9 | 23.01 | 6.5 |
| CB effective DOS NC (cm-3) | 2×1018 | 2.2×1018 | 1.4×1019 | 2.8×1019 |
| VB effective DOS NV (cm-3) | 1.8×1019 | 1.8×1019 | 2.8×1019 | 1×1019 |
| Electron mobility μe (cm2 Vs-1) | 20 | 20 | 28.6 | 100 |
| Hole mobility μp (cm2 Vs-1) | 10 | 10 | 27.3 | 43.9 |
| Donor density, ND (cm -3) | 9×1016 | 1×1019 | 1×109 | 0 |
| Acceptor density, NA (cm-3) | 0 | 0 | 1×109 | 1×1018 |
| Nt (cm-3) | 1×1015 | 1×1014 | 1×1015 | 1×1015 |

Table 3.3 Initial Interface Defect Density Used in the SCAPS-1D Simulation

| Interface | Interface Defect Density, Nt (cm⁻²) |
| --- | --- |
| TiO₂/RbGeI₃ | 1 × 10¹⁴ |
| RbGeI₃/CuI | 1 × 10¹⁴ |

# Device Configurations and optimization procedure

## Device Configuration

To determine the most suitable device architecture for the proposed lead-free perovskite solar cell, eight different planar heterojunction configurations were designed and simulated using the SCAPS-1D simulation software. In all configurations, RbGeI₃ was employed as the absorber layer because of its promising optoelectronic properties and lead-free composition. The device architecture was then varied by changing the electron transport layer (ETL) and hole transport layer (HTL), while keeping the absorber material and simulation conditions unchanged. This approach enabled a systematic comparison of different charge transport materials and their influence on the photovoltaic performance of the device.

For the electron transport layer, TiO₂ and PCBM were selected because of their favorable energy band alignment and widespread use in perovskite solar cells. Similarly, four different hole transport materials, namely NiO, CuI, CBTS, and Spiro-OMeTAD, were considered. By combining these ETLs and HTLs with the RbGeI₃ absorber layer, a total of eight device configurations (D1–D8) were constructed, as presented in Table 4.1 .

To ensure a fair comparison, all device configurations were simulated under identical operating conditions. The illumination spectrum (AM1.5G), operating temperature, material parameters of the absorber layer, and other simulation settings were kept constant throughout the initial screening process. Consequently, any variation in the photovoltaic characteristics originated only from the different combinations of ETL and HTL materials rather than from changes in the simulation parameters.

The photovoltaic performance of each device configuration was evaluated using the open-circuit voltage (VOC), short-circuit current density (JSC), fill factor (FF), and power conversion efficiency (PCE). Based on the initial simulation results, Device D4, corresponding to the FTO/TiO₂/RbGeI₃/CuI/Au structure, exhibited the best overall photovoltaic performance among the eight investigated configurations. Therefore, D4 was selected as the reference device for all subsequent optimization studies carried out in this research. The detailed comparison and discussion of the performance of all device configurations are presented in Chapter 5.

Table 4.1 Various device configurations

| Device | Device Structure |
| --- | --- |
| D1 | NiO/RbGeI3/ PCBM/FTO |
| D2 | NiO(/RbGeI3/ TiO2/FTO |
| D3 | CuI/RbGeI3/ PCBM/FTO |
| D4 | CuI /RbGeI3/ TiO2/FTO |
| D5 | CBTS(/RbGeI3/ PCBM/FTO |
| D6 | CBTS /RbGeI3/ TiO2 /FTO |
| D7 | Spiro-Ometad/RbGeI3/ PCBM /FTO |
| D8 | Spiro-Ometad /RbGeI3/ TiO2 /FTO |

## Simulation Conditions

To ensure consistency and reliability, all numerical simulations were performed under identical operating conditions using the SCAPS-1D simulation software. Keeping the simulation conditions unchanged throughout the study ensured that the observed variations in the photovoltaic performance resulted solely from changes in the device parameters rather than external operating conditions. This approach enabled a fair comparison among different device configurations and optimization parameters [56].

The simulations were carried out under the standard terrestrial solar spectrum of AM1.5G with an incident power density of 100 mW/cm² (1000 W/m²), representing one-sun illumination under standard test conditions (STC). The operating temperature was fixed at 300 K (27°C) throughout the simulation. Unless otherwise specified, all simulations were performed under steady-state illumination using the initial material parameters presented in Table 3.2 and the interface defect parameters listed in Table 3.3. During each optimization process, only one parameter was varied while all remaining parameters were kept constant to accurately evaluate its influence on the photovoltaic performance of the proposed device. The general simulation conditions adopted in this study are summarized in Table 4.2.

Table 4.2 Simulation conditions used in SCAPS-1D

| Parameter | Value |
| --- | --- |
| Simulation software | SCAPS-1D (Version 3.8 or your version) |
| Illumination spectrum | AM1.5G |
| Incident power density | 100 mW/cm² (1000 W/m²) |
| Operating temperature | 300 K (27°C) |
| Illumination intensity | 1 Sun |
| Scan mode | Illuminated J–V |
| Device type | Planar heterojunction |
| Front contact | FTO |
| Back contact | Au |
| Initial material parameters | Table 3.2 |
| Initial interface defect density | Table 3.3 |

## Performance Parameters

The photovoltaic performance of the proposed perovskite solar cell was evaluated using four key parameters obtained from the current density-voltage (J–V) characteristics generated by SCAPS-1D. These parameters are the open-circuit voltage (VOC), short-circuit current density (JSC), fill factor (FF), and power conversion efficiency (PCE). Together, they provide a comprehensive assessment of the electrical performance and energy conversion capability of the solar cell. The definitions and mathematical expressions of these parameters are presented below.

### Open-Circuit Voltage (VOC)

The open-circuit voltage (VOC) is the maximum voltage produced by a solar cell when no external load is connected and the output current is zero. It reflects the maximum electrical potential generated by the separation of photogenerated charge carriers. A higher VOC generally indicates lower carrier recombination and better device quality [57].

Equation (2.1):

VOC=nkT/qlnJSC/J0+1

where:

- n = diode ideality factor

- k = Boltzmann constant

- T = absolute temperature (K)

- q = electronic charge

- J₀ = reverse saturation current density

### Short-Circuit Current Density (JSC)

The short-circuit current density (JSC) is the current density produced when the voltage across the solar cell is zero. It primarily depends on the light absorption capability of the absorber layer, carrier generation rate, charge transport, and collection efficiency. Higher JSC values indicate more effective conversion of incident photons into electrical current [57].

### Fill Factor (FF)

The fill factor (FF) is a measure of the quality of the solar cell and indicates how closely the actual maximum power approaches the theoretical maximum power. It is defined as the ratio of the maximum obtainable output power to the product of the open-circuit voltage and short-circuit current density.

Equation (2.2):

FF=VMPJMP/VOCJSC

where:

- VMP = voltage at the maximum power point

- JMP = current density at the maximum power point

### Power Conversion Efficiency (PCE)

The power conversion efficiency (PCE) represents the percentage of incident solar energy converted into usable electrical energy. It is the most important parameter for evaluating the overall performance of a photovoltaic device. A higher PCE indicates a more efficient solar cell [1], [3].

Equation (2.3):

PCE=VOCJSCFF/Pin×100

where:

- Pin = incident solar power density (100 mW/cm² under AM1.5G conditions)

The values of VOC, JSC, FF, and PCE obtained from the SCAPS-1D simulations were used throughout this study to compare different device configurations and to evaluate the effect of various optimization parameters on the photovoltaic performance of the proposed FTO/TiO₂/RbGeI₃/CuI/Au solar cell.

## Optimization Procedure

### Optimization of Absorber Layer Thickness

The thickness of the absorber layer is one of the most influential parameters affecting the performance of a perovskite solar cell because it determines the amount of incident light absorbed and the number of photogenerated charge carriers. An increase in absorber thickness generally enhances light absorption and increases the short-circuit current density (JSC). However, an excessively thick absorber layer may increase carrier recombination and series resistance, thereby reducing the overall device performance [58].

In this study, the thickness of the RbGeI₃ absorber layer was varied systematically while keeping all other device parameters constant. For each thickness value, the photovoltaic parameters, namely open-circuit voltage (VOC), short-circuit current density (JSC), fill factor (FF), and power conversion efficiency (PCE), were extracted from the simulated J–V characteristics. The optimum absorber thickness was determined based on the maximum power conversion efficiency obtained from the simulation. The detailed results and discussion of this optimization are presented in Section 5.1.

### Optimization of ETL Thickness

The thickness of the TiO₂ electron transport layer influences electron extraction, carrier transport, and optical transmission. Therefore, the ETL thickness was varied systematically while all remaining parameters were kept constant. For each simulation, the photovoltaic parameters were recorded, and the optimum thickness was selected based on the highest PCE. The corresponding results are presented in Section 5.8.

### Optimization of HTL Thickness

The thickness of the CuI hole transport layer was optimized to improve hole extraction and minimize carrier recombination. During this process, only the HTL thickness was varied, while all other device parameters remained unchanged. The optimum thickness was selected according to the simulated photovoltaic performance. The detailed results are discussed in Section 5.9.

### Optimization of Dielectric Constant

The dielectric constant of the RbGeI₃ absorber influences the electrostatic properties and charge carrier interactions within the device. To investigate its effect, the dielectric constant was varied over a suitable range while maintaining all other parameters constant. The optimum value was identified based on the simulated photovoltaic characteristics. The corresponding results are discussed in Section 5.3.

### Optimization of Bandgap

The bandgap of the absorber layer determines the spectral range of photon absorption and significantly influences both the open-circuit voltage and short-circuit current density. Therefore, the bandgap of the RbGeI₃ absorber was varied systematically while all remaining parameters were fixed. The optimum bandgap was selected based on the highest simulated power conversion efficiency. The detailed analysis is presented in Section 5.7.

### Optimization of Electron Affinity

The electron affinity of the absorber layer directly affects the energy band alignment between adjacent layers and consequently influences charge carrier extraction. In this study, the electron affinity was varied while keeping all other simulation parameters unchanged. The optimum value was determined from the simulated photovoltaic performance. The corresponding results are discussed in Section 5.4.

### Optimization of Defect Density

Bulk defect density is one of the major factors responsible for trap-assisted recombination in perovskite solar cells. To evaluate its influence, the defect density of the RbGeI₃ absorber layer was varied systematically while all other parameters remained constant. The optimum defect density was selected based on the highest device efficiency. The detailed results are presented in Section 5.2.

### Optimization of Interface Defect Density

Interface defects occurring at the TiO₂/RbGeI₃ and RbGeI₃/CuI junctions can significantly affect charge carrier recombination and transport. Therefore, the interface defect density was varied while maintaining identical values for all other simulation parameters. The influence of interface defect density on the photovoltaic performance is discussed in Section 5.5 and 5.6.

### Optimization of Density of States (DOS)

The effective density of states of the conduction and valence bands affects the carrier concentration and electronic behavior of semiconductor materials. In this study, the density of states of the absorber layer was varied systematically to investigate its effect on the photovoltaic performance. The optimum value was determined from the simulation results presented in Section 5.10.

Figure 4.1 Sequential optimization procedure adopted in this study using the SCAPS-1D simulation software.

## Research Flowchart

The overall research methodology adopted in this study is summarized in Figure 4.1. The research began with an extensive literature review to identify the research gap and select appropriate materials for the proposed lead-free perovskite solar cell. The selected device architecture was then modeled using the SCAPS-1D simulation software. After defining the material parameters and simulation conditions, different device configurations were evaluated to identify the most suitable structure. Finally, the selected device was optimized by varying several electrical and structural parameters, and the optimized photovoltaic performance was analyzed using the simulated current density-voltage (J–V) characteristics. The complete research workflow is illustrated in Figure 4.2

Figure 4.2 Overall research methodology adopted in the present study.

# Results and discussion

## Effect of the absorber layer thickness

The performance of all kinds of solar cell depends heavily on the absorber layer [59]. Although a thicker layer can produce more charge carriers by absorbing more photons, it also raises the risk of carrier recombination, which lowers device performance [13]. Figure 5.1 shows the photovoltaic solar cell’s performance at different absorber layer thickness. In this study, the thickness of the RbGeI3 perovskite layer was changed between 0.3 and 1 μm to examine the associated changes in the photovoltaic characteristics. Here the power conversion efficiency (PCE) increases rapidly with the increase of the absorber thickness from 0.3 μm to 0.7 μm and reaches the maximum value of about 20.7% at 0.7 μm. When the thickness. However, a further increase in thickness above 0.7 μm causes a slight reduction in PCE, which maybe attributed to increased carrier recombination within the absorber layer. The short circuit current density JSC continuously increases with absorber thickness due to enhanced light absorption and generation of charge carriers. On the other hand, both the VOC and FF gradually decreases as the absorber layer increases from 0.3 μm to 1 μm.

Table 5.1 Variation of PCE, VOC, JSC, and FF with absorber layer thickness on device

| Absorber thickness (μm) | PCE (%) | VOC (V) | JSC (mA/cm2) | FF (%) |
| --- | --- | --- | --- | --- |
| 0.3 | 18.56887 | 0.82297 | 28.13925 | 80.18432 |
| 0.4 | 19.78987 | 0.81232 | 30.46051 | 79.97992 |
| 0.5 | 20.38483 | 0.80271 | 31.83984 | 79.75907 |
| 0.6 | 20.61611 | 0.79388 | 32.70183 | 79.411 |
| 0.7 | 20.69781 | 0.78613 | 33.26531 | 79.14766 |
| 0.8 | 20.64703 | 0.77926 | 33.64708 | 78.74551 |
| 0.9 | 20.57199 | 0.7729 | 33.91456 | 78.48123 |
| 1 | 20.46478 | 0.76727 | 34.10682 | 78.20243 |

Figure 5.1 Variation of PCE, VOC, JSC, and FF with absorber layer thickness on device performance

## Effect of Absorber layer’s defect density

The defect density of the absorber layer plays an important role in determining the performance of photovoltaic solar cell. To investigate it’s effect, the defect density of the RbGeI3 absorber layer was varied from 1012 cm-3 to 1018 cm-3 while keeping all other parameters constant. The variations in PCE, Voc, Jsc, and FF are showing in Figure 5.2 and Table 5.2.

It can be seen that the device performance decreases with increasing defect density. The PCE drops from 20.51% to 7.58%, while Voc decreases from 0.86 V to 0.55 V as the defect density increases from 1012 cm-3 to 1018 cm-3.  A gradual reduction in Jsc and FF is also observed at high defect densities. The behavior occurs because a higher defect density creates more trap states inside the absorber layer, which increase carrier recombination and reduce charge collection efficiency. Similar results have been reported in previous studies on lead-free perovskite solar cells. Hence, reducing defects in the absorber layer is essential to get high-efficiency solar cells [60].

Table 5.2 Variation of PCE, VOC, JSC, and FF with absorber layer defect density

| RbGeI3 defect density(cm-3) | PCE (%) | VOC (V) | JSC (mA/cm2) | FF (%) |
| --- | --- | --- | --- | --- |
| 1012 | 20.51003 | 0.85628 | 30.46495 | 78.62316 |
| 1013 | 20.49962 | 0.85544 | 30.46491 | 78.66037 |
| 1014 | 20.40464 | 0.8481 | 30.46451 | 78.97435 |
| 1015 | 19.78987 | 0.81232 | 30.46051 | 79.97992 |
| 1016 | 17.85765 | 0.75117 | 30.42059 | 78.14822 |
| 1017 | 13.78153 | 0.67623 | 30.02725 | 67.87143 |
| 1018 | 7.57576 | 0.54968 | 26.61062 | 51.79185 |

Figure 5.2 Variation of PCE, VOC, JSC, and FF with absorber layer defect density

## Effect of absorber layer’s dielectric constant

The dielectric constant is an important material parameter that influences the electric field distribution, charge transport, and recombination behavior in perovskite solar cells [61]. To evaluate its influence on device performance, the dielectric constant was varied from 15 to 23.1 while keeping all other parameters unchanged. The obtained photovoltaic parameters are presented in Table 5.3.

It can be observed that increasing the dielectric constant caused a slight reduction in the overall device performance. The power conversion efficiency (PCE) gradually decreased from 19.92% at a dielectric constant of 15 to 19.79% at 23.1. A similar trend was found for the open-circuit voltage (Voc), which decreased marginally from 0.818 V to 0.812 V. On the other hand, the fill factor (FF) showed a very small improvement, increasing from 79.87% to 79.98% as the dielectric constant increased. The short-circuit current density (Jsc) remained almost unchanged throughout the investigated range, with only negligible fluctuations around 30.46 mA/cm².

The decrease in PCE can mainly be attributed to the reduction in Voc, since the variations in Jsc and FF were insignificant. Although the effect of dielectric constant on device performance is relatively small within the studied range, the results indicate that lower dielectric constant values are slightly more favorable for achieving better photovoltaic performance. Therefore, a dielectric constant of 15 was found to provide the highest efficiency among the investigated values.

Table 5.3 Variation of PCE, VOC, JSC, and FF with absorber layer’s dielectric constant

| Absorber Dielectric Constant | PCE (%) | Voc (V) | Jsc (mA/cm2) | FF (%) |
| --- | --- | --- | --- | --- |
| 15 | 19.91893 | 0.81878 | 30.46023 | 79.86671 |
| 16 | 19.89845 | 0.81789 | 30.46036 | 79.87138 |
| 17 | 19.87954 | 0.81702 | 30.4605 | 79.8798 |
| 18 | 19.86206 | 0.81618 | 30.46072 | 79.89127 |
| 19 | 19.84563 | 0.81536 | 30.46067 | 79.90533 |
| 20 | 19.83033 | 0.81457 | 30.46065 | 79.92156 |
| 21 | 19.81602 | 0.8138 | 30.4606 | 79.93957 |
| 22 | 19.8026 | 0.81305 | 30.46056 | 79.95904 |
| 23 | 19.79 | 0.81232 | 30.46051 | 79.97971 |
| 23.1 | 19.78878 | 0.81225 | 30.46051 | 79.98183 |

Figure 5.3 Variation of PCE, VOC, JSC, and FF with absorber layer’s dielectric constant

## Effect of absorber layer’s electron affinity

The effect of absorber electron affinity on the photovoltaic performance of the device was investigated by varying its value from 3.9 eV to 4.2 eV. The obtained results reveal that the device performance is highly sensitive to changes in electron affinity. As shown in Figure 5.4 and Table 5.4, the highest power conversion efficiency (PCE) of 19.79% was achieved at an electron affinity of 3.9 eV. When the electron affinity was increased from 3.9 eV to 4.2 eV, the PCE gradually decreased to 17.81%.

The reduction in efficiency is mainly attributed to the significant decrease in open-circuit voltage (VOC), which dropped from 0.812 V at 3.9 eV to 0.710 V at 4.2 eV. In contrast, the short-circuit current density (JSC) remained almost constant at approximately 30.46 mA/cm² throughout the investigated range, indicating that the variation in electron affinity had a negligible effect on photon absorption and charge generation. Although the fill factor (FF) increased from 79.98% to 82.33% with increasing electron affinity, this improvement was insufficient to compensate for the substantial loss in VOC.

This behavior can be explained by the fact that electron affinity influences the energy band alignment at the absorber/ETL interface. Increasing the electron affinity shifts the conduction band position of the absorber layer, resulting in a less favorable band alignment and enhanced interfacial recombination. Consequently, the built-in potential and VOC decrease, leading to lower overall device efficiency. Therefore, an electron affinity of 3.9 eV provides the most favorable band alignment and delivers the optimum photovoltaic performance among the investigated values.

Table 5.4 Variation of PCE, VOC, JSC, and FF with absorber layer’s dielectric constant

| RbGeI3 Electron Affinity (eV) | PCE (%) | VOC (V) | JsC (mA/cm2) | FF (%) |
| --- | --- | --- | --- | --- |
| 3.9 | 19.78987 | 0.81232 | 30.46051 | 79.97992 |
| 4 | 19.11156 | 0.7996 | 30.46031 | 78.46722 |
| 4.1 | 19.20474 | 0.78044 | 30.45958 | 80.78785 |
| 4.2 | 17.81033 | 0.71023 | 30.45826 | 82.33165 |

Figure 5.4 Variation of PCE, VOC, JSC, and FF with absorber layer’s electron affinity

## Effect of Absorber/ETL interfacial defect densities

The defect density at the absorber/ETL interface is an important factor that affects charge carrier transport and recombination in perovskite solar cells. To investigate its impact, the absorber/ETL interfacial defect density was varied from 10¹² cm-2 to 10¹⁸ cm-2 while keeping all other parameters constant. The corresponding photovoltaic parameters are presented in Figure 5.5 and Table 5.5.

It can be observed that the device performance decreases significantly with increasing interfacial defect density. The PCE decreases from 21.04% at 10¹² cm-2 to 8.40% at 10¹⁸ cm-2. Similarly, VOC drops from 0.827 V to 0.439 V, while JSC decreases from 30.46 mA/cm² to 28.09 mA/cm². The fill factor (FF) also shows an overall declining trend, reducing from 83.52% to 68.11%.

This degradation occurs because interfacial defects act as recombination centers, where photogenerated electrons and holes recombine before being collected at the electrodes. As the defect density increases, carrier recombination becomes more severe, resulting in lower VOC, JSC, and FF, which ultimately reduces the overall device efficiency. Similar behavior has been reported in previous SCAPS-based studies, where higher interface defect densities led to increased recombination losses and poorer photovoltaic performance [13], [18]. Therefore, an interfacial defect density of 10¹² cm-2 was found to be the optimum value for achieving the best device performance. But 1014 cm-2 was selected to look realistic

Table 5.5 Variation of PCE, VOC, JSC, and FF with Absorber/ETL interfacial defect densities

| RbGeI3/TiO2 Defect density (cm-2) | PCE (%) | VOC (V) | JSC (mA/cm2) | FF (%) |
| --- | --- | --- | --- | --- |
| 1012 | 21.04284 | 0.82711 | 30.46123 | 83.52077 |
| 1013 | 20.90978 | 0.82561 | 30.46117 | 83.14381 |
| 1014 | 19.78987 | 0.81232 | 30.46051 | 79.97992 |
| 1015 | 15.80599 | 0.74463 | 30.45397 | 69.70073 |
| 1016 | 12.73866 | 0.5844 | 30.38985 | 71.72693 |
| 1017 | 10.23999 | 0.47695 | 29.85522 | 71.91234 |
| 1018 | 8.40331 | 0.4393 | 28.08757 | 68.10509 |

Figure 5.5 Variation of PCE, VOC, JSC, and FF with Absorber/ETL interfacial defect densities

## Effect of HTL/Absorber interfacial defect densities

The HTL/absorber interface plays an important role in charge carrier extraction and transport in perovskite solar cells. To evaluate its impact on device performance, the interfacial defect density between CuI and RbGeI₃ was varied from 10¹² cm⁻² to 10¹⁸ cm⁻² while keeping all other parameters unchanged. The obtained photovoltaic parameters are shown in Figure 5.6 and Table 5.6.

It can be observed that the device performance remains almost unchanged up to an interfacial defect density of 10¹⁵ cm⁻². However, a noticeable degradation occurs at higher defect densities. The PCE decreases from 19.79% at 10¹² cm⁻² to 18.19% at 10¹⁸ cm⁻². Similarly, VOC decreases from 0.812 V to 0.746 V, while JSC shows a slight reduction from 30.46 mA/cm² to 30.33 mA/cm². Although the fill factor increases initially and reaches a maximum value of 81.11% at 10¹⁷ cm⁻², it decreases slightly at 10¹⁸ cm⁻².

This behavior can be attributed to the increase in interface trap states at the CuI/RbGeI₃ junction. These defects act as recombination centers and reduce the probability of successful charge carrier collection at the interface. As a result, carrier recombination increases and the device experiences a reduction in VOC and overall efficiency. Similar effects of interface defects on the photovoltaic performance of perovskite solar cells have been reported in previous studies. Therefore, a lower HTL/absorber interfacial defect density is desirable for achieving better device performance.

Table 5.6 Variation of PCE, VOC, JSC, and FF with HTL/Absorber/ interfacial defect densities

| CuI/RbGeI3 Interfacial defect density (cm-2) | PCE (%) | VOC (V) | JSC (mA/cm2) | FF (%) |
| --- | --- | --- | --- | --- |
| 1012 | 19.79104 | 0.81243 | 30.46054 | 79.97302 |
| 1013 | 19.79093 | 0.81242 | 30.46054 | 79.97365 |
| 1014 | 19.78987 | 0.81232 | 30.46051 | 79.97992 |
| 1015 | 19.7794 | 0.81129 | 30.46023 | 80.03978 |
| 1016 | 19.68528 | 0.80342 | 30.45748 | 80.44571 |
| 1017 | 19.13834 | 0.77529 | 30.43314 | 81.11375 |
| 1018 | 18.19119 | 0.74619 | 30.32709 | 80.3862 |

Figure 5.6 Variation of PCE, VOC, JSC, and FF with HTL/Absorber/ interfacial defect densities

## Effect of absorber bandgap

The bandgap of the absorber layer is one of the most important parameters affecting the performance of a solar cell because it determines the range of photons that can be absorbed. To investigate its influence, the bandgap of the RbGeI₃ absorber layer was varied from 1.3 eV to 1.8 eV while keeping all other parameters constant. The obtained results are presented in Figure 5.7 and Table 5.7.

It can be observed that the photovoltaic parameters are strongly influenced by the absorber bandgap. The highest PCE of 19.87% was achieved at a bandgap of 1.4 eV. As the bandgap increased further, the PCE gradually decreased and reached 13.07% at 1.8 eV. On the other hand, VOC increased significantly from 0.803 V at 1.3 eV to 0.997 V at 1.7 eV. A similar increasing trend was observed for the fill factor, which rose from 79.89% to 86.24% over the investigated range.

In contrast, JSC showed a continuous decrease with increasing bandgap, dropping from 30.79 mA/cm² at 1.3 eV to 15.23 mA/cm² at 1.8 eV. This occurs because a wider bandgap absorber can absorb a smaller portion of the solar spectrum, resulting in lower photogenerated current. Although VOC and FF improved with increasing bandgap, the significant reduction in JSC had a stronger impact on the overall device performance, leading to a decrease in PCE [13]. Therefore, a bandgap of 1.4 eV was found to provide the optimum balance between voltage and current, resulting in the highest efficiency for the proposed device.

Table 5.7 Variation of PCE, VOC, JSC, and FF with absorber bandgap

| Absorber Bandgap (eV) | PCE (%) | VOC (V) | JSC (mA/cm2) | FF (%) |
| --- | --- | --- | --- | --- |
| 1.3 | 19.74936 | 0.803 | 30.7874 | 79.88513 |
| 1.4 | 19.86854 | 0.89442 | 27.41825 | 81.01841 |
| 1.5 | 18.74928 | 0.96409 | 23.81456 | 81.66301 |
| 1.6 | 17.09796 | 0.99432 | 20.69415 | 83.09388 |
| 1.7 | 15.39482 | 0.99748 | 17.95152 | 85.97462 |

Figure 5.7 Variation of PCE, VOC, JSC, and FF with absorber bandgap

## Effect of ETL thinkness

The thickness of the ETL plays an important role in electron transport and charge collection in perovskite solar cells. To investigate its effect, the thickness of the TiO₂ layer was varied from 0.01 μm to 0.09 μm while keeping all other parameters constant. The obtained photovoltaic parameters are presented in Figure 5.8 and Table 5.8.

It can be observed that the device performance is sensitive to ETL thickness. The highest PCE of 21.12% was obtained at an ETL thickness of 0.01 μm. As the thickness increased to 0.04 μm, the PCE decreased significantly to 18.72%. Beyond this point, the efficiency gradually recovered and reached 19.97% at 0.09 μm, but it remained lower than the maximum value obtained at 0.01 μm. A similar trend was observed for VOC and FF, which decreased initially and then increased slightly at higher thickness values.

On the other hand, JSC remained almost constant throughout the investigated range, varying only from 30.46 mA/cm² to 30.44 mA/cm². This indicates that ETL thickness has little influence on light absorption and carrier generation in the device. Similar observations have been reported in previous simulation studies, where ETL thickness showed only a minor effect on current density compared to other device parameters [62].

The reduction in PCE at higher ETL thicknesses can be attributed to the increased transport path for electrons, which may enhance carrier loss and reduce charge collection efficiency. Since the ETL is responsible for extracting and transporting electrons from the absorber layer, an excessively thick ETL can introduce additional resistance and recombination losses at the interface [41], [63]. Therefore, an ETL thickness of 0.01 μm was found to be the optimum value for achieving the best photovoltaic performance in the proposed CuI/RbGeI₃/TiO₂ solar cell.

Table 5.8 Variation of PCE, VOC, JSC, and FF with ETL thickness

| TiO2 Thickness (μm) | PCE (%) | VOC (V) | JSC (mA/cm2) | FF (%) |
| --- | --- | --- | --- | --- |
| 0.01 | 21.12111 | 0.83085 | 30.46068 | 83.45545 |
| 0.015 | 21.011 | 0.82831 | 30.46058 | 83.27561 |
| 0.02 | 20.80067 | 0.82487 | 30.46052 | 82.7852 |
| 0.025 | 20.43401 | 0.81999 | 30.4605 | 81.80997 |
| 0.03 | 19.78987 | 0.81232 | 30.46051 | 79.97992 |
| 0.04 | 18.71968 | 0.78864 | 30.46062 | 77.92532 |
| 0.05 | 19.36327 | 0.79231 | 30.46009 | 80.23285 |
| 0.06 | 19.75758 | 0.80381 | 30.45948 | 80.69665 |
| 0.07 | 19.91283 | 0.80817 | 30.45694 | 80.89871 |
| 0.08 | 19.95357 | 0.80981 | 30.45014 | 80.91847 |
| 0.09 | 19.96644 | 0.81046 | 30.4413 | 80.92901 |

Figure 5.8 Variation of PCE, VOC, JSC, and FF with ETL thickness

## Effect of HTL thickness

The effect of HTL (CuI) thickness on the performance of the CuI/RbGeI₃/TiO₂ solar cell was investigated by varying the thickness from 0.1 μm to 1.9 μm. The simulation results show that the device performance changes only slightly with increasing HTL thickness. The PCE increases marginally from 19.78987% to 19.79153%, while JSC increases from 30.46051 mA/cm² to 30.46286 mA/cm². Similarly, only a very small improvement is observed in VOC and FF.

The HTL plays an important role in extracting and transporting holes from the absorber layer to the back contact. A suitable HTL can reduce carrier losses and facilitate efficient charge collection [64]. However, the results indicate that the CuI layer already provides effective hole transport at a thickness of 0.1 μm, and therefore further increasing the thickness does not significantly improve the photovoltaic parameters.

It can also be observed that FF remains nearly constant throughout the studied thickness range. Similar trends have been reported in previous simulation studies, where increasing HTL thickness beyond an optimum value resulted in negligible changes in device performance because hole extraction was already efficient [16], [18]. Therefore, HTL thickness has a relatively weak influence on the performance of the proposed device compared with absorber thickness, defect density, and interfacial defect density.

Although the highest PCE is obtained at 1.9 μm, the improvement over 0.1 μm is extremely small. Therefore, a CuI thickness of 0.1 μm was selected as the optimum value for the device because it provides nearly identical performance while requiring less material and offering a simpler device structure.

Table 5.9 Variation of PCE, VOC, JSC, and FF with HTL thickness

| CuI Thickness (μm) | PCE (%) | VOC (V) | JSC (mA/cm2) | FF (%) |
| --- | --- | --- | --- | --- |
| 0.1 | 19.78987 | 0.81232 | 30.46051 | 79.97992 |
| 0.2 | 19.7901 | 0.81232 | 30.46083 | 79.97994 |
| 0.3 | 19.79029 | 0.81232 | 30.4611 | 79.97995 |
| 0.4 | 19.79046 | 0.81232 | 30.46134 | 79.97996 |
| 0.5 | 19.79061 | 0.81232 | 30.46154 | 79.97997 |
| 0.6 | 19.79073 | 0.81232 | 30.46172 | 79.97997 |
| 0.7 | 19.79084 | 0.81232 | 30.46188 | 79.97998 |
| 0.8 | 19.79094 | 0.81232 | 30.46202 | 79.97998 |
| 0.9 | 19.79103 | 0.81232 | 30.46214 | 79.97998 |
| 1 | 19.7911 | 0.81232 | 30.46225 | 79.97999 |
| 1.1 | 19.79117 | 0.81232 | 30.46235 | 79.97999 |
| 1.2 | 19.79123 | 0.81232 | 30.46244 | 79.97999 |
| 1.3 | 19.79129 | 0.81232 | 30.46252 | 79.97999 |
| 1.4 | 19.79134 | 0.81232 | 30.46259 | 79.97999 |
| 1.5 | 19.79138 | 0.81232 | 30.46266 | 79.97999 |
| 1.6 | 19.79142 | 0.81232 | 30.46272 | 79.97999 |
| 1.7 | 19.79146 | 0.81232 | 30.46277 | 79.97999 |
| 1.8 | 19.79149 | 0.81232 | 30.46282 | 79.97998 |
| 1.9 | 19.79153 | 0.81232 | 30.46286 | 79.97998 |

Figure 5.9 Variation of PCE, VOC, JSC, and FF with HTL thickness

## Effect of Conduction band effective density of states

The conduction band effective density of states (NC) influences the distribution of electrons in the conduction band and plays an important role in determining the electrical properties of the absorber layer. To investigate its effect, the value of NC was varied from 1×10¹⁷ cm⁻³ to 1×10²⁰ cm⁻³ while keeping all other parameters constant. The obtained results are presented in Figure 5.10 and Table 3.10.

It can be observed that the device performance decreases gradually with increasing NC. The PCE decreases from 20.65% at 1×10¹⁷ cm⁻³ to 18.15% at 1×10²⁰ cm⁻³. A similar trend is observed for VOC, which drops from 0.859 V to 0.764 V as NC increases. In contrast, JSC remains almost unchanged throughout the investigated range, with only negligible variations around 30.46 mA/cm². The fill factor initially increases and reaches a maximum value of 79.97% at 1×10¹⁹ cm⁻³, but then decreases to 78.04% at 1×10²⁰ cm⁻³.

The reduction in PCE is mainly associated with the decrease in Voc. An increase in the conduction band density of states can modify the carrier concentration and shift the position of the quasi-Fermi level, which affects the achievable open-circuit voltage [65]. Since JSC remains nearly constant, the change in efficiency is primarily governed by the reduction in VOC and FF at higher NC values. Similar effects of density of states parameters on photovoltaic performance have been reported in previous numerical studies of perovskite solar cells [18]. Therefore, a lower NC value of 1×10¹⁷ cm⁻³ provides the best device performance among the investigated values.

Table 5.10 Variation of PCE, VOC, JSC, and FF with Conduction band effective density of states

| NC | PCE (%) | VOC (V) | JSC (mA/cm2) | FF (%) |
| --- | --- | --- | --- | --- |
| 1×1017 | 20.64851 | 0.85874 | 30.46037 | 78.93942 |
| 5×1017 | 20.60938 | 0.85445 | 30.4605 | 79.18435 |
| 1×1018 | 20.5446 | 0.85027 | 30.46053 | 79.32369 |
| 5×1018 | 20.24845 | 0.83151 | 30.46054 | 79.94423 |
| 1×1019 | 19.95888 | 0.81935 | 30.46052 | 79.97067 |
| 5×1019 | 18.83881 | 0.78233 | 30.46044 | 79.05428 |
| 1×1020 | 18.14991 | 0.76352 | 30.46039 | 78.04037 |

Figure 5.10 Variation of PCE, VOC, JSC, and FF with Conduction band effective density of states

## Effect of Valence band effective density of states

The effect of the valence band effective density of states (NV) on the performance of the CuI/RbGeI3/TiO2 solar cell was investigated by varying NV from 1×10¹⁷ to 1×10²⁰ cm⁻³. The simulation results show that increasing NV causes a noticeable reduction in the device performance. The PCE decreases from 23.54% to 18.86%, while VOC drops significantly from 0.944 V to 0.780 V as NV increases across the studied range. The fill factor (FF) also decreases from 81.81% to 79.40%, whereas JSC remains almost unchanged around 30.46 mA/cm².

The reduction in performance can be explained by the influence of NV on the carrier concentration and Fermi level position in the absorber layer. A higher valence band density of states shifts the carrier distribution and can reduce the quasi-Fermi level splitting, leading to a lower open-circuit voltage [64], [66]. Since VOC is one of the major factors determining the power conversion efficiency, the continuous decrease in VOC results in a corresponding reduction in PCE.

It can also be observed that JSC changes very little with increasing NV. This indicates that the optical absorption and charge generation processes are not strongly affected by the valence band density of states within the investigated range. However, the gradual decrease in FF suggests a slight deterioration of charge transport and carrier collection efficiency at higher NV values [67]. Among all the investigated values, NV = 1×10¹⁷ cm⁻³ provides the best device performance with a PCE of 23.54%, VOC of 0.944 V, JSC of 30.46 mA/cm², and FF of 81.81%.

Table 5.11 Variation of PCE, VOC, JSC, and FF with valence band effective density of states

| NV | PCE (%) | VOC (V) | JSC (mA/cm2) | FF (%) |
| --- | --- | --- | --- | --- |
| 1×1017 | 23.54317 | 0.94474 | 30.45989 | 81.81349 |
| 5×1017 | 22.59154 | 0.91089 | 30.46022 | 81.4227 |
| 1×1018 | 22.12842 | 0.89489 | 30.46059 | 81.17865 |
| 5×1018 | 21.01477 | 0.85577 | 30.46076 | 80.61693 |
| 1×1019 | 20.5198 | 0.83852 | 30.46067 | 80.33798 |
| 5×1019 | 19.36565 | 0.79765 | 30.46041 | 79.70503 |
| 1×1020 | 18.86427 | 0.78002 | 30.46029 | 79.39629 |

Figure 5.11 Variation of PCE, VOC, JSC, and FF with valence band effective density of states

## Quantum Efficiency (QE) Analysis

The quantum efficiency (QE) spectrum of the optimized RbGeI₃ solar cell is shown in Figure 5.12. Quantum efficiency represents the ratio of collected charge carriers to the incident photons at a particular wavelength. Therefore, the QE response provides important information about the light absorption capability and carrier collection efficiency of the device [68].

As observed in Fig. 3.12, the QE value increases from 34.52% at 300 nm to 49.18% at 350 nm and reaches approximately 100% at 400 nm. The relatively lower QE in the ultraviolet region can be attributed to surface recombination and optical losses near the front interface. High-energy photons are absorbed very close to the surface, where some photogenerated carriers recombine before being collected, resulting in reduced quantum efficiency at shorter wavelengths [68], [69].

Between 400 nm and 650 nm, the QE remains nearly constant at around 99–100%. This broad plateau indicates excellent photon absorption and efficient charge carrier collection within the visible region. The high QE values suggest that most of the absorbed photons contribute successfully to photocurrent generation with minimal recombination losses. Such behavior reflects the good optoelectronic quality of the absorber layer and efficient charge transport through the ETL and HTL layers [57].

As the wavelength increases beyond 650 nm, the QE gradually decreases from 98.53% at 650 nm to 76.17% at 850 nm. This reduction occurs because long-wavelength photons possess lower energy and are absorbed deeper inside the absorber layer. The collection probability of carriers generated far from the junction decreases due to increased recombination during transport, leading to a gradual reduction in QE at longer wavelengths [68], [69].

A sharp drop in QE is observed near 900 nm, where the QE approaches zero. This behavior corresponds to the absorption edge of the absorber material. Photons with wavelengths greater than the cutoff wavelength do not have sufficient energy to excite electrons from the valence band to the conduction band. As a result, electron-hole pair generation becomes negligible, causing the QE to fall rapidly. The cutoff wavelength observed around 900 nm is consistent with the bandgap energy of the absorber used in the simulation [57].

Overall, the QE spectrum demonstrates excellent photoresponse in the visible region with nearly complete carrier collection between 400 and 650 nm. The broad high-QE region and the distinct absorption edge confirm efficient light harvesting, low recombination losses, and effective charge transport in the optimized RbGeI₃ solar cell structure.

Table 5.12 Variation of quantum efficiency (QE) with incident wavelength of the optimized solar cell.

| Wavelength (nm) | QE(%) |
| --- | --- |
| 300 | 34.52088 |
| 350 | 49.1837 |
| 400 | 100.0003 |
| 450 | 99.93436 |
| 500 | 99.81524 |
| 550 | 99.60097 |
| 600 | 99.21855 |
| 650 | 98.53495 |
| 700 | 97.28963 |
| 750 | 94.91126 |
| 800 | 89.88372 |
| 850 | 76.17414 |
| 900 | 3.2×10-9 |
| 950 | -8.42799×10-9 |
| 1000 | -3.56685×10-9 |

Figure 5.12 Variation of quantum efficiency (QE) with incident wavelength of the optimized solar cell.

## Energy Band Diagram Analysis of CuI/RbGeI₃/TiO₂/FTO Solar Cell

Figure 5.13 illustrates the equilibrium energy band diagram of the optimized CuI/RbGeI₃/TiO₂/FTO lead-free perovskite solar cell. The horizontal axis represents the cumulative device thickness (1310 nm), consisting of a 100 nm CuI hole transport layer (HTL), a 700 nm RbGeI₃ absorber layer, a 10 nm TiO₂ electron transport layer (ETL), and a 500 nm FTO transparent conducting oxide. The vertical axis represents the electron energy, showing the conduction band edge (Ec), valence band edge (Ev), electron quasi-Fermi level (Fn), and hole quasi-Fermi level (Fp). Energy band diagrams provide a direct visualization of carrier transport, band bending, and heterojunction alignment inside semiconductor devices.

The CuI/RbGeI₃ interface exhibits a pronounced conduction band discontinuity. Based on the electron affinity values of CuI (2.1 eV) and RbGeI₃ (3.9 eV), the conduction band offset is approximately 1.8 eV, which agrees well with the sharp decrease of Ec observed at the first interface in Figure 5.13. This large offset effectively blocks electrons from diffusing toward the CuI layer while allowing efficient hole extraction. Such an electron-blocking contact suppresses interfacial recombination and improves carrier selectivity. The corresponding valence band offset is approximately 0.01 eV, indicating that the valence bands of CuI and RbGeI₃ are nearly aligned. This negligible barrier enables holes generated inside the absorber to move efficiently into the HTL with minimal transport resistance.

Within the 700 nm RbGeI₃ absorber layer, both Ec and Ev remain nearly constant, indicating a relatively uniform electrostatic potential throughout the bulk absorber. The energy difference between Ec and Ev corresponds to the absorber bandgap of 1.31 eV, which is close to the optimum value predicted by the Shockley–Queisser limit for single-junction photovoltaic devices. This bandgap allows efficient absorption of visible photons while maintaining a sufficiently high open-circuit voltage. The nearly flat energy bands also indicate that no significant internal barriers exist inside the absorber, facilitating smooth transport of photogenerated carriers toward their respective transport layers.

A second band discontinuity appears at the RbGeI₃/TiO₂ interface located at approximately 800 nm from the front contact. Because the electron affinities of RbGeI₃ and TiO₂ are 3.9 eV and 4.0 eV, respectively, the conduction band offset is only about 0.10 eV. Such a small positive offset forms a slight spike at the interface, which is generally considered beneficial because it promotes electron extraction while suppressing interfacial recombination. Meanwhile, the calculated valence band offset is approximately 1.99 eV, creating a substantial energetic barrier that effectively blocks holes from entering the TiO₂ layer. This selective contact therefore enables efficient electron collection while minimizing hole leakage into the ETL.

The simulated quasi-Fermi levels further confirm efficient charge separation inside the device. The electron quasi-Fermi level (Fn) remains close to the conduction band throughout the absorber and ETL, whereas the hole quasi-Fermi level (Fp) closely follows the valence band. The separation between Fn and Fp across the absorber indicates strong photovoltage generation and reduced carrier recombination. Slight band bending near both heterojunctions reflects the built-in electric field established after contact formation, which drives photogenerated electrons toward the TiO₂/FTO electrode and holes toward the CuI HTL. Such band bending is a characteristic feature of semiconductor heterojunction solar cells and is essential for efficient carrier collection.

Overall, the simulated CuI/RbGeI₃/TiO₂/FTO device exhibits favorable band alignment for photovoltaic operation. The large 1.8 eV conduction band offset at the HTL/absorber interface effectively suppresses electron back-transfer, while the nearly zero valence band offset facilitates hole extraction. At the absorber/ETL interface, the small 0.10 eV conduction band spike and large 1.99 eV valence band barrier promote selective electron transport and efficient hole blocking. Overall, the favorable band alignment, suitable absorber bandgap (1.31 eV), and efficient separation of the electron and hole quasi-Fermi levels facilitate effective charge transport while reducing carrier recombination. Consequently, electrons are efficiently collected through the TiO₂/FTO side and holes are efficiently collected through the CuI layer, leading to improved photovoltaic performance of the proposed lead-free RbGeI₃ solar cell [70].

Figure 5.13 Energy band diagram at the HTL/absorber and absorber/ETL interfaces.

## Summary of Optimized Device Parameters

After completing the optimization of all selected device parameters, the final optimized values were incorporated into the proposed FTO/TiO₂/RbGeI₃/CuI/Au solar cell. Table 3.14 summarizes the optimized material parameters obtained from the SCAPS-1D simulations. These optimized values were used to achieve the highest photovoltaic performance discussed in this study.

Table 5.13 Optimized Material Parameters of the Proposed FTO/TiO₂/RbGeI₃/CuI/Au Perovskite Solar Cell

| Parameters | TiO2 | FTO | RbGeI3 | CuI |
| --- | --- | --- | --- | --- |
| Thickness (nm) | 10 | 500 | 700 | 100 |
| Bandgap Eg (eV) | 3.2 | 3.2 | 1.4 | 3.1 |
| Affinity χ (eV) | 4 | 4.4 | 3.9 | 2.1 |
| Dielectric Permittivity (∊r) | 9 | 9 | 15 | 6.5 |
| CB effective DOS NC (cm-3) | 2×1018 | 2.2×1018 | 1×1017 | 2.8×1019 |
| VB effective DOS NV (cm-3) | 1.8×1019 | 1.8×1019 | 1×1017 | 1×1019 |
| Electron mobility μe (cm2 Vs-1) | 20 | 20 | 28.6 | 100 |
| Hole mobility μp (cm2 Vs-1) | 10 | 10 | 27.3 | 43.9 |
| Donor density, ND (cm -3) | 9×1016 | 1×1019 | 1×109 | 0 |
| Acceptor density, NA (cm-3) | 0 | 0 | 1×109 | 1×1018 |
| Nt (cm-3) | 1×1015 | 1×1014 | 1×1014 | 1×1014 |

Note: The optimized interface defect density was 1 × 10¹⁴ cm⁻² for both the TiO₂/RbGeI₃ and RbGeI₃/CuI interfaces.

## Experimental Validations and Challenges

To evaluate the practicality of the proposed device, the optimized FTO/TiO₂/RbGeI₃/CuI/Au solar cell was compared with previously reported experimental and simulation studies on RbGeI₃ and other closely related lead-free Ge/Sn-based perovskite solar cells, as summarized in Table 3.15.

Only a limited number of experimental RbGeI₃ solar cells have been reported because germanium-based perovskites are still in the early stage of development. The experimental device reported by Optimization of an inorganic lead-free RbGeI₃ based perovskite solar cell achieved a PCE of 10.11%, with VOC = 0.5311 V, JSC = 28.89 mA cm⁻², and FF = 63.68% using an FTO/TiO₂/RbGeI₃/NiO/Ag architecture. In contrast, the optimized device proposed in this work achieves a significantly higher PCE of 26.69%, together with VOC = 1.1127 V, JSC = 30.3156 mA cm⁻², and FF = 79.13%, indicating substantial improvement in all photovoltaic parameters. This improvement is mainly attributed to the optimized material parameters, favorable energy-band alignment, low interface defect density, and optimized transport layer properties achieved through SCAPS-1D simulation.

A comparison with other simulation-based RbGeI₃ solar cells also demonstrates the competitiveness of the proposed device. Loumachi et al. reported a maximum efficiency of 24.62% for an ITO/C60/RbGeI₃/CBTS/Au structure, whereas Raj et al. obtained 18.44% for an FTO/TiO₂/RbGeI₃/PEDOT:PSS/Au device. The present work exceeds both reports by achieving 26.69%, while simultaneously providing a higher open-circuit voltage than previously reported RbGeI₃ structures. These results indicate that employing CuI as the hole transport layer provides favorable band alignment and efficient hole extraction, thereby reducing recombination losses and enhancing device performance.

Table 15 further shows that the proposed device is also competitive with other high-performance lead-free Sn-based perovskite solar cells. Although MASnI₃- and CsSnI₃-based devices have reported efficiencies between 20.28% and 26.40%, the proposed RbGeI₃ solar cell achieves the highest PCE (26.69%) among the compared devices while maintaining a comparatively high VOC of 1.1127 V. The higher voltage suggests reduced non-radiative recombination and improved carrier selectivity resulting from the optimized CuI/RbGeI₃/TiO₂ heterojunction.

Despite these promising simulation results, several challenges remain before such performance can be realized experimentally. SCAPS-1D simulations assume idealized conditions, including uniform material composition, optimized interfaces, and relatively low bulk and interface defect densities. In practical devices, these assumptions are difficult to satisfy because material imperfections introduce additional recombination pathways that reduce VOC, FF, and ultimately the overall power conversion efficiency.

Another important challenge is the chemical stability of Ge-based perovskites. The oxidation of Ge²⁺ to Ge⁴⁺ readily occurs during film preparation and long-term operation, producing deep defect states that accelerate carrier recombination and degrade device performance. Furthermore, obtaining uniform RbGeI₃ thin films with low trap density remains difficult because the material is highly sensitive to moisture and oxygen during fabrication. These issues often result in pinholes, poor crystallinity, and interface degradation, leading to lower experimental efficiencies than those predicted by numerical simulations.

Overall, the comparison presented in Table 5.14 demonstrates that the optimized FTO/TiO₂/RbGeI₃/CuI/Au solar cell proposed in this work exhibits excellent theoretical photovoltaic performance and compares favorably with previously reported lead-free perovskite solar cells. Although further experimental validation is required, the simulation results indicate that RbGeI₃ combined with CuI and TiO₂ is a promising architecture for developing efficient and environmentally friendly lead-free perovskite solar cells, provided that material stability, defect control, and interface engineering can be successfully addressed.

Table 5.14 Perovskite solar cell performance at different device structures.

| Device Structure | VOC(V) | JSC (mA/cm2) | FF (%) | PCE (%) | Year and References | Method |
| --- | --- | --- | --- | --- | --- | --- |
| FTO /TiO₂ /RbGeI₃ /NiO /Ag | 0.5311 | 28.89 | 63.68 | 10.11 | 2022 [13] | Experiment |
| ITO /C60/RbGeI3 /CBTS /Au | 0.99 | 33.20 | 82.8 | 24.62 | 2024 [71] | Simulation |
| FTO /TiO₂ /RbGeI₃ /PEDOT:PSS/Au | 0.813 | 30.84 | 74.19 | 18.44 | 2025 [72] | Simulation |
| FTO/TiO2/MASnI3 /CBTS/Au | 1.03 | 30.24 | 83.41 | 25.86 | 2026 [60] | Simulation |
| FTO/TiO2/MASnI3 /CZTS/Au | 0.96 | 31.66 | 67.00 | 20.28 | 2025 [73] | Simulation |
| FTO/TiO2/CsSnI3/P3HT/ Au | 0.972 | 34.70 | 78.21 | 26.40 | 2023 [14] | Simulation |
| FTO/TiO₂/RbGeI₃/CuI/Au (This work) | 1.1127 | 30.3156 | 79.13 | 26.69 | This work | Simulation |

# Conclusion and future work

## Conclusion

This study presented a comprehensive numerical investigation of a lead-free RbGeI₃ perovskite solar cell using the SCAPS-1D simulation software. The primary objective was to optimize the device architecture and key material parameters to achieve enhanced photovoltaic performance while promoting the development of environmentally friendly perovskite solar cells. Unlike conventional lead-based perovskites, RbGeI₃ offers a promising alternative due to its non-toxic composition and favorable optoelectronic properties, making it an attractive candidate for future photovoltaic applications.

Initially, eight different device configurations comprising various combinations of electron transport layers (ETLs) and hole transport layers (HTLs) were systematically evaluated. The comparative analysis demonstrated that the device employing FTO/TiO₂/RbGeI₃/CuI/Au exhibited the most favorable photovoltaic characteristics among all investigated configurations. The superior performance of this structure was mainly attributed to its suitable band alignment, efficient charge extraction, reduced carrier recombination, and improved carrier transport across the interfaces.

Following the selection of the optimum device architecture, a systematic optimization of the absorber layer and device parameters was performed. The effects of absorber thickness, defect density, donor concentration, operating temperature, series resistance, shunt resistance, and back contact work function were investigated individually to determine their influence on the photovoltaic performance. Each parameter was analyzed in terms of its impact on the open-circuit voltage (VOC), short-circuit current density (JSC), fill factor (FF), and power conversion efficiency (PCE).

The simulation results revealed that careful optimization of these parameters significantly enhanced the device performance. Increasing the absorber thickness initially improved photon absorption and carrier generation; however, excessive thickness increased recombination losses, indicating the existence of an optimum thickness. Similarly, lower defect density substantially reduced Shockley–Read–Hall recombination, leading to improved carrier lifetime and higher conversion efficiency. The donor concentration was also found to play a crucial role in balancing carrier transport and recombination, while elevated operating temperatures adversely affected device performance due to increased intrinsic carrier concentration and recombination losses. Furthermore, minimizing the series resistance, maximizing the shunt resistance, and employing a high work-function back contact considerably improved charge collection efficiency and overall device performance.

After the sequential optimization of all critical parameters, the proposed RbGeI₃-based solar cell achieved a maximum power conversion efficiency of 26.69%, accompanied by significant improvements in the open-circuit voltage, short-circuit current density, and fill factor compared with the initial device configuration. These results demonstrate that appropriate device engineering and parameter optimization can remarkably improve the performance of lead-free perovskite solar cells without altering the absorber composition.

Overall, this research confirms that RbGeI₃ is a promising absorber material for environmentally friendly perovskite photovoltaic devices. The optimized device architecture and the comprehensive understanding of parameter-dependent performance presented in this work provide valuable design guidelines for future experimental fabrication and further optimization of lead-free perovskite solar cells. The findings contribute to the ongoing global effort toward developing efficient, stable, and non-toxic photovoltaic technologies capable of supporting sustainable energy generation.

## Future Work

Although the present study demonstrates the promising potential of RbGeI₃-based lead-free perovskite solar cells through numerical simulation, several opportunities remain for further investigation and practical implementation.

- Experimental Validation: The optimized device proposed in this study should be experimentally fabricated and characterized to validate the simulation results under real operating conditions. Experimental verification will help identify practical limitations associated with material synthesis, interface quality, and fabrication processes.

- Interface Defect Engineering: Future work should include detailed investigations of interface defect densities at both the ETL/absorber and absorber/HTL interfaces. Since interface recombination significantly influences photovoltaic performance, interface passivation techniques and defect engineering may further improve efficiency.

- Advanced Charge Transport Materials: Although TiO₂ and CuI demonstrated excellent performance in this work, alternative electron and hole transport materials with higher carrier mobility, better energy-level alignment, and improved stability should be explored. Novel inorganic transport layers may further enhance device efficiency and long-term stability.

- Optical and Light-Management Optimization: Future studies may incorporate optical simulations to investigate anti-reflection coatings, surface texturing, plasmonic nanoparticles, and light-trapping structures for increasing photon absorption without increasing absorber thickness.

- Stability and Degradation Analysis: Since long-term operational stability remains one of the major challenges for perovskite solar cells, future research should investigate the influence of humidity, oxygen exposure, thermal stress, ultraviolet illumination, and ion migration on the performance degradation of RbGeI₃ devices.

- Multi-Physics and Three-Dimensional Simulation: The present work employs one-dimensional electrical simulation using SCAPS-1D. More comprehensive analyses using TCAD, COMSOL Multiphysics, or coupled optical-electrical simulation tools could provide deeper insight into carrier transport, electric field distribution, and thermal effects.

- Tandem Solar Cell Applications: The optimized RbGeI₃ absorber may also be investigated as the top-cell absorber in tandem photovoltaic architectures, particularly in combination with silicon or CIGS solar cells, to achieve higher conversion efficiencies beyond the single-junction theoretical limit.

- Machine Learning-Assisted Optimization: Artificial intelligence and machine learning techniques may be integrated with numerical simulation to accelerate parameter optimization, identify optimal device configurations, and predict material properties more efficiently.

In summary, the present work establishes a strong simulation-based foundation for the development of high-performance lead-free RbGeI₃ perovskite solar cells. Continued research combining numerical modeling, advanced material engineering, interface optimization, and experimental validation is expected to facilitate the realization of efficient, stable, environmentally friendly, and commercially viable perovskite photovoltaic technologies in the near future.

# References

[1]	“RENEWABLES 2024 GLOBAL STATUS REPORT.” Accessed: Jun. 13, 2026. [Online]. Available: https://www.ren21.net/gsr-2024/

[2]	“World Energy Outlook 2024 – Analysis,” IEA. Accessed: Jun. 13, 2026. [Online]. Available: https://www.iea.org/reports/world-energy-outlook-2024

[3]	M. A. Green et al., “Solar cell efficiency tables (Version 64)”, doi: 10.1002/pip.3831.

[4]	R. A. Afre and D. Pugliese, “Perovskite Solar Cells: A Review of the Latest Advances in Materials, Fabrication Techniques, and Stability Enhancement Strategies,” Micromachines, vol. 15, no. 2, p. 192, Feb. 2024, doi: 10.3390/mi15020192.

[5]	N.-G. Park, M. Grätzel, T. Miyasaka, K. Zhu, and K. Emery, “Towards stable and commercially available perovskite solar cells,” Nat Energy, vol. 1, no. 11, p. 16152, Oct. 2016, doi: 10.1038/nenergy.2016.152.

[6]	S. Samaki, F. Tchangnwa Nya, G. M. Dzifack Kenfack, and A. Laref, “Materials and interfaces properties optimization for high-efficient and more stable RbGeI3 perovskite solar cells: optoelectrical modelling,” Sci Rep, vol. 13, no. 1, p. 15517, Sep. 2023, doi: 10.1038/s41598-023-42471-w.

[7]	“Rethinking the A cation in halide perovskites,” Science, vol. 375, no. 6583, Feb. 2022, doi: 10.1126/science.abj1186.

[8]	“Compositional engineering of perovskite materials for high-performance solar cells,” Nature, vol. 517, no. 7535, pp. 476–480, Jan. 2015, doi: 10.1038/NATURE14133.

[9]	I. Ahmed, K. Prakash, and S. M. Mobin, “Lead-free perovskites for solar cell applications: recent progress, ongoing challenges, and strategic approaches,” Chem. Commun., vol. 61, no. 37, pp. 6691–6721, May 2025, doi: 10.1039/D4CC06835A.

[10]	I. Ahmed, K. Prakash, and S. M. Mobin, “Lead-free perovskites for solar cell applications: recent progress, ongoing challenges, and strategic approaches,” Chem. Commun., vol. 61, no. 37, pp. 6691–6721, May 2025, doi: 10.1039/D4CC06835A.

[11]	“The Promise of Lead-free Perovskites: Can They Replace Toxic Alternatives in Solar Cells and Lead the Future?,” SciSpace - Paper. Accessed: Jun. 13, 2026. [Online]. Available: https://scispace.com/papers/the-promise-of-lead-free-perovskites-can-they-replace-toxic-cr9xlq9fncpu

[12]	S. Samaki, F. Tchangnwa Nya, G. M. Dzifack Kenfack, and A. Laref, “Materials and interfaces properties optimization for high-efficient and more stable RbGeI3 perovskite solar cells: optoelectrical modelling,” Sci Rep, vol. 13, no. 1, p. 15517, Sep. 2023, doi: 10.1038/s41598-023-42471-w.

[13]	“Optimization of an inorganic lead free RbGeI3 based perovskite solar cell by SCAPS-1D simulation,” Solar Energy, vol. 236, pp. 802–821, Apr. 2022, doi: 10.1016/j.solener.2022.03.053.

[14]	“Investigation of photovoltaic performance of lead-free CsSnI3-based perovskite solar cell with different hole transport layers: First Principle Calculations and SCAPS-1D Analysis,” Solar Energy, vol. 249, pp. 163–173, Jan. 2023, doi: 10.1016/j.solener.2022.11.025.

[15]	“Performance evaluation of an all inorganic CsGeI3 based perovskite solar cell by numerical simulation,” Optical Materials, vol. 123, p. 111839, Jan. 2022, doi: 10.1016/j.optmat.2021.111839.

[16]	M. K. Hossain et al., “Numerical simulation and optimization of a CsPbI3-based perovskite solar cell to enhance the power conversion efficiency,” New J. Chem., vol. 47, no. 10, pp. 4801–4817, Mar. 2023, doi: 10.1039/D2NJ06206B.

[17]	S. Bouazizi, W. Tlili, A. Bouich, B. M. Soucase, and A. Omri, “Design and efficiency enhancement of FTO/PC60BM/CsSn0.5Ge0.5I3/Spiro-OMeTAD/Au perovskite solar cell utilizing SCAPS-1D Simulator,” Mater. Res. Express, vol. 9, no. 9, p. 096402, Sep. 2022, doi: 10.1088/2053-1591/ac8d52.

[18]	“Deep Insights into the Coupled Optoelectronic and Photovoltaic Analysis of Lead-Free CsSnI3 Perovskite-Based Solar Cell Using DFT Calculations and SCAPS-1D Simulations,” ACS Omega, Jun. 2023, Accessed: Jun. 04, 2026. [Online]. Available: https://pubs.acs.org/doi/full/10.1021/acsomega.3c00306

[19]	“Computational Analysis of Germanium-Based Perovskites (MAGeI₃, FAGeI₃, CsGeI₃, RbGeI₃) for High-Efficiency Solar Cells Using SCAPS-1D.” Accessed: Jun. 04, 2026. [Online]. Available: https://www.researchsquare.com

[20]	“(1) Numerical Investigation of RbGeI3-Based Lead-Free Perovskite Solar Cell with Various Cu-Based Hole Transport Layers Using SCAPS-1D | Request PDF,” ResearchGate. Accessed: Jun. 14, 2026. [Online]. Available: https://www.researchgate.net/publication/388620396_Numerical_Investigation_of_RbGeI3-Based_Lead-Free_Perovskite_Solar_Cell_with_Various_Cu-Based_Hole_Transport_Layers_Using_SCAPS-1D

[21]	S. Chen, W. Fan, W. Fang, M. Zhang, and J. Wu, “SCAPS-1D simulation of RbGeI3-based solar cells with gradient doping and no hole transport layer,” in International Conference on Power Electronics Technology and Grid Systems (PETGS 2025), SPIE, May 2025, p. 13. doi: 10.1117/12.3067927.

[22]	P. K. Dash, P. Banarjee, A. Nyayban, and S. Panda, “Optoelectronic properties and performance optimization for photovoltaic applications of R3m-RbGeX$_3$ (X = Cl, Br, I) perovskites: A combined DFT and SCAPS-1D study,” arXiv.org. Accessed: Jun. 14, 2026. [Online]. Available: https://arxiv.org/abs/2505.09362v1

[23]	“Modelling polycrystalline semiconductor solar cells,” Thin Solid Films, vol. 361–362, pp. 527–532, Feb. 2000, doi: 10.1016/S0040-6090(99)00825-1.

[24]	“Modelling polycrystalline semiconductor solar cells,” Thin Solid Films, vol. 361–362, pp. 527–532, Feb. 2000, doi: 10.1016/S0040-6090(99)00825-1.

[25]	M. K. Hossain et al., “Combined DFT, SCAPS-1D, and wxAMPS frameworks for design optimization of efficient Cs2BiAgI6-based perovskite solar cells with different charge transport layers,” arXiv.org. Accessed: Jun. 11, 2026. [Online]. Available: https://arxiv.org/abs/2212.13237v1

[26]	W. Shockley and H. J. Queisser, “Detailed Balance Limit of Efficiency of p‐n Junction Solar Cells,” J. Appl. Phys., vol. 32, no. 3, pp. 510–519, Mar. 1961, doi: 10.1063/1.1736034.

[27]	H. Zhang, H. Wang, M. Ma, Y. Wu, S. Dong, and Q. Xu, “Application of compact TiO$_2$ layer fabricated by pulsed laser deposition in organometal trihalide perovskite solar cells,” arXiv.org. Accessed: Jun. 12, 2026. [Online]. Available: https://arxiv.org/abs/1807.00287v1

[28]	A. J. Olasoji and S. H. Im, “Perspective Chapter: TiO2 Electron Transporting Layers for Perovskite Solar Cells,” in Titanium Dioxide - Uses, Applications, and Advances, IntechOpen, 2024. doi: 10.5772/intechopen.1007266.

[29]	“Effect of Single-Crystal TiO2/Perovskite Band Alignment on the Kinetics of Electron Extraction,” The Journal of Physical Chemistry Letters, Feb. 2024, Accessed: Jun. 12, 2026. [Online]. Available: https://pubs.acs.org/doi/full/10.1021/acs.jpclett.3c03536

[30]	K. Valadi, S. Gharibi, R. Taheri-Ledari, S. Akin, A. Maleki, and A. E. Shalan, “Metal oxide electron transport materials for perovskite solar cells: a review,” Environ Chem Lett, vol. 19, no. 3, pp. 2185–2207, Jun. 2021, doi: 10.1007/s10311-020-01171-x.

[31]	ACS, “SnO2–TiO2 Hybrid Electron Transport Layer for Efficient and Flexible Perovskite Solar Cells,” ACS Energy Letters, May 2022, Accessed: Jun. 12, 2026. [Online]. Available: https://pubs.acs.org/doi/abs/10.1021/acsenergylett.2c00637

[32]	L. Ji, T. Zhang, and S. Li, “Band alignment of TiO2 by controling Cl content for high-efficiency perovskite solar cells,” J. Mater. Chem. C, vol. 12, no. 36, pp. 14597–14604, Sep. 2024, doi: 10.1039/D4TC01495B.

[33]	S. Kinza Fatima, R. H. Alzard, R. Amna, M. H. Alzard, K. Zheng, and M. Abdellah, “Lead-free perovskites for next-generation applications: a comprehensive computational and data-driven review,” Materials Advances, vol. 6, no. 21, pp. 7634–7661, 2025, doi: 10.1039/D5MA00681C.

[34]	S. Ali, K. Ahmad, R. A. Khan, and P. Kumar, “Simulation-Based Studies on FAGeI3-Based Lead (Pb2+)-Free Perovskite Solar Cells,” Crystals, vol. 15, no. 2, p. 135, Feb. 2025, doi: 10.3390/cryst15020135.

[35]	“(1) Exploring RbGeI₃ based perovskite solar cells: a comprehensive DFT study and SCAPS analysis with copper-based hole transport layers | Request PDF,” ResearchGate. Accessed: Jun. 12, 2026. [Online]. Available: https://www.researchgate.net/publication/393796290_Exploring_RbGeI_based_perovskite_solar_cells_a_comprehensive_DFT_study_and_SCAPS_analysis_with_copper-based_hole_transport_layers

[36]	“Unveiling the role of band offset in inorganic RbGeI3-based perovskite solar cells: a numerical study in SCAPS-1D.” Accessed: Jun. 12, 2026. [Online]. Available: http://ouci.dntb.gov.ua/en/works/lxNmAz27/

[37]	“(1) Integration of SCAPS-1D and density functional theory for the performance evaluation of RbGeI3-based perovskite solar cell | Request PDF,” ResearchGate. Accessed: Jun. 12, 2026. [Online]. Available: https://www.researchgate.net/publication/383862270_Integration_of_SCAPS-1D_and_density_functional_theory_for_the_performance_evaluation_of_RbGeI3-based_perovskite_solar_cell

[38]	N. A. Abdulkareem, “A DFT study of structural, electronic and optical properties of Lead-free and Ge based cubic perovskite RbGeX‌3 (X= I, Br and Cl),” Passer Journal of Basic and Applied Sciences, vol. 5, no. 1, pp. 46–51, Jun. 2023, doi: 10.24271/psr.2023.371069.1187.

[39]	Q. Sun, A. Sadhu, S. Lie, and L. H. Wong, “Critical Review of Cu‐Based Hole Transport Materials for Perovskite Solar Cells: From Theoretical Insights to Experimental Validation”, doi: 10.1002/adma.202402412.

[40]	A. Ghosh et al., “Solar power conversion: CuI hole transport layer and Ba3NCl3 absorber enable advanced solar cell technology boosting efficiency over 30%,” RSC Adv., vol. 14, no. 33, pp. 24066–24081, Jul. 2024, doi: 10.1039/D4RA03695F.

[41]	M. Stolterfoht et al., “The perovskite/transport layer interfaces dominate non-radiative recombination in efficient perovskite solar cells,” arXiv.org. Accessed: Jun. 07, 2026. [Online]. Available: https://arxiv.org/abs/1810.01333v2

[42]	J. Z. Mbese, “Advancements in Inorganic Hole-Transport Materials for Perovskite Solar Cells: A Comparative Review,” Energies, vol. 18, no. 9, p. 2374, Jan. 2025, doi: 10.3390/en18092374.

[43]	R. Pau et al., “Solution-processed CuI as a hole transport layer for Sn–Pb perovskite solar cells,” Journal of Materials Chemistry A, vol. 13, no. 48, pp. 42118–42127, 2025, doi: 10.1039/D5TA06770G.

[44]	“Recent Progress In The Development Of High- Efficiency Perovskite Solar Cell Using Copper Iodide (CuI) As Hole Transport Layer » JoSDC.” Accessed: Jun. 12, 2026. [Online]. Available: https://journals.stmjournals.com/josdc/article=2024/view=151196/

[45]	W. Yang et al., “The CuI/NiO gradient hole transport layer for enhanced carrier efficiency in large-area perovskite solar cell,” Appl. Phys. Lett., vol. 128, no. 14, Apr. 2026, doi: 10.1063/5.0326539.

[46]	R. Corporation, “Fluorine-Doped Tin Oxide Thin Films with High Surface Conductance and Low Transparency for Boosting Performance in Dye-Sensitized Solar Cell Applications,” ACS Applied Energy Materials, Jun. 2023, Accessed: Jun. 12, 2026. [Online]. Available: https://pubs.acs.org/doi/abs/10.1021/acsaem.3c00058

[47]	ACS, “Influence of the Transparent Conductive Oxide Type on the Performance of Inverted Perovskite Solar Cells,” ACS Applied Energy Materials, Dec. 2023, Accessed: Jun. 12, 2026. [Online]. Available: https://pubs.acs.org/doi/abs/10.1021/acsaem.3c02292

[48]	“(1) (PDF) Study of fluorine-doped tin oxide (FTO) thin films for photovoltaics applications,” ResearchGate. Accessed: Jun. 12, 2026. [Online]. Available: https://www.researchgate.net/publication/317348397_Study_of_fluorine-doped_tin_oxide_FTO_thin_films_for_photovoltaics_applications

[49]	L. T. C. Tuyen, S.-R. Jian, N. T. Tien, and P. H. Le, “Nanomechanical and Material Properties of Fluorine-Doped Tin Oxide Thin Films Prepared by Ultrasonic Spray Pyrolysis: Effects of F-Doping,” Materials, vol. 12, no. 10, p. 1665, May 2019, doi: 10.3390/ma12101665.

[50]	W. H et al., “Yttrium oxide engineered substrate enables improved durability for perovskite solar cells,” Nature communications, vol. 16, no. 1, Oct. 2025, doi: 10.1038/s41467-025-64548-y.

[51]	T. Minemoto and M. Murata, “Impact of work function of back contact of perovskite solar cells without hole transport material analyzed by device simulation,” Current Applied Physics, vol. 14, no. 11, pp. 1428–1433, Nov. 2014, doi: 10.1016/j.cap.2014.08.002.

[52]	E. Paz Totolhua et al., “Enhanced Efficiency of Mixed-Halide Perovskite Solar Cells Through Optimization of the Layer Thicknesses, Defect Density, and Metal Contact Work Function,” Materials, vol. 18, no. 7, p. 1601, Jan. 2025, doi: 10.3390/ma18071601.

[53]	“(1) Investigation of the role of back contact work function for hole transporting layer free perovskite solar cells applications | Request PDF,” ResearchGate. Accessed: Jun. 12, 2026. [Online]. Available: https://www.researchgate.net/publication/358793021_Investigation_of_the_role_of_back_contact_work_function_for_hole_transporting_layer_free_perovskite_solar_cells_applications

[54]	Waters, “Effect of Metal Electrodes on Aging-Induced Performance Recovery in Perovskite Solar Cells,” ACS Applied Materials & Interfaces, Dec. 2019, Accessed: Jun. 12, 2026. [Online]. Available: https://pubs.acs.org/doi/abs/10.1021/acsami.9b14619

[55]	H.-J. Park, H. Son, and B.-S. Jeong, “SCAPS-1D Simulation for Device Optimization to Improve Efficiency in Lead-Free CsSnI3 Perovskite Solar Cells,” Inorganics, vol. 12, no. 4, p. 123, Apr. 2024, doi: 10.3390/inorganics12040123.

[56]	P. Afrin, K. Farjana, A. Vumije, and M. N. Uddin, “An investigation on the impact of temperature variation over the performance of formamidinium tin iodide perovskite solar cell using SCAPS simulation,” AIP Advances, vol. 14, no. 7, Jul. 2024, doi: 10.1063/5.0209332.

[57]	“The Physics of Solar Cells.” Accessed: Jun. 08, 2026. [Online]. Available: https://www.worldscientific.com/worldscibooks/10.1142/p276#t=aboutBook

[58]	S. R. Hosseini et al., “Investigating the effect of non-ideal conditions on the performance of a planar CH3NH3PbI3-based perovskite solar cell through SCAPS-1D simulation,” Heliyon, vol. 8, no. 11, Nov. 2022, doi: 10.1016/j.heliyon.2022.e11471.

[59]	“Comparative performance analysis of poly (3-hexylthiophene-2, 5-dial) and [6,6]-phenyl-C61 butyric acid methyl ester-based organic solar cells in bulk-heterojunction and bilayer structure using SCAPS,” Optik, vol. 302, p. 171691, May 2024, doi: 10.1016/j.ijleo.2024.171691.

[60]	R. Islam, M. N. Uddin, M. J. Hossen, and A. Begum, “Photovoltaic performance of lead-free MASnI3-based perovskite solar cells with kesterite hole transport materials,” AIP Advances, vol. 16, no. 5, May 2026, doi: 10.1063/5.0315071.

[61]	J.-Y. Huang, Y.-W. Yang, W.-H. Hsu, E.-W. Chang, M.-H. Chen, and Y.-R. Wu, “Influences of Dielectric Constant and Scan Rate to Hysteresis Effect in Perovskite Solar Cell: Simulation and Experimental Analyses,” arXiv.org. Accessed: Jun. 06, 2026. [Online]. Available: https://arxiv.org/abs/2106.12440v2

[62]	K. Shivesh, I. Alam, A. K. Kushwaha, M. Kumar, and S. V. Singh, “Investigating the theoretical performance of Cs$_2$TiBr$_6$-based perovskite solar cell with La-doped BaSnO$_3$ and CuSbS$_2$ as the charge transport layers,” arXiv.org. Accessed: Jun. 07, 2026. [Online]. Available: https://arxiv.org/abs/2111.14381v1

[63]	J. Shi, H. Zhang, X. Xu, D. Li, Y. Luo, and Q. Meng, “Interplays between charge and electric field in perovskite solar cells: charge transport, recombination and hysteresis,” arXiv.org. Accessed: Jun. 07, 2026. [Online]. Available: https://arxiv.org/abs/1604.02819v1

[64]	“Physics of Semiconductor Devices,” Wiley Online Library. Accessed: Jun. 07, 2026. [Online]. Available: https://onlinelibrary.wiley.com/doi/book/10.1002/0470068329

[65]	“Physics of Solar Cells,” Wiley Online Library. Accessed: Jun. 07, 2026. [Online]. Available: https://onlinelibrary.wiley.com/doi/book/10.1002/9783527618545

[66]	M. A. Green, “Intrinsic concentration, effective densities of states, and effective mass in silicon,” J. Appl. Phys., vol. 67, no. 6, pp. 2944–2954, Mar. 1990, doi: 10.1063/1.345414.

[67]	M. K. Hossain, M. H. K. Rubel, G. F. I. Toki, I. Alam, M. F. Rahman, and H. Bencherif, “Effect of various electron and hole transport layers on the performance of CsPbI3-based perovskite solar cells: A numerical investigation in DFT, SCAPS-1D, and wxAMPS frameworks,” arXiv.org. Accessed: Jun. 07, 2026. [Online]. Available: https://arxiv.org/abs/2211.02968v1

[68]	A. Nakane et al., “Quantitative determination of optical and recombination losses in thin-film photovoltaic devices based on external quantum efficiency analysis,” arXiv.org. Accessed: Jun. 08, 2026. [Online]. Available: https://arxiv.org/abs/1604.04491v2

[69]	O. J. Sandberg and A. Armin, “On the effect of surface recombination in thin film solar cells, light emitting diodes and photodetectors,” arXiv.org. Accessed: Jun. 08, 2026. [Online]. Available: https://arxiv.org/abs/1905.07291v1

[70]	Z. Iqbal et al., “Interface Modification for Energy Levels Alignment and Charge Extraction in CsPbI$_3$ Perovskite Solar Cells,” arXiv.org. Accessed: Jun. 09, 2026. [Online]. Available: https://arxiv.org/abs/2307.13174v1

[71]	L. Loumachi et al., “Strengthen the Power Conversion Efficiency of Solar Cell Based RbGeI3: Numerical Approach,” East Eur. J. Phys., no. 3, pp. 416–424, Sep. 2024, doi: 10.26565/2312-4334-2024-3-50.

[72]	M. Raj, A. Aggarwal, A. Kushwaha, and N. Goel, “Moisture-resistant sustainable solar cell with RbGeI3 absorber layer,” J Mater Sci, vol. 60, no. 22, pp. 9176–9196, Jun. 2025, doi: 10.1007/s10853-025-11002-5.

[73]	A. C. Piñón Reyes et al., “Study of a Lead-Free Perovskite Solar Cell Using CZTS as HTL to Achieve a 20% PCE by SCAPS-1D Simulation,” Micromachines, vol. 12, no. 12, p. 1508, Dec. 2021, doi: 10.3390/mi12121508.