# Tables (editable)

Table 1. Eight device configurations screened in this study. All configurations were simulated at an absorber thickness of 400 nm.

| Device | Architecture |
| --- | --- |
| D1 | FTO / PCBM / RbGeI_3 / NiO / Au |
| D2 | FTO / TiO_2 / RbGeI_3 / NiO / Au |
| D3 | FTO / PCBM / RbGeI_3 / CuI / Au |
| D4 | FTO / TiO_2 / RbGeI_3 / CuI / Au |
| D5 | FTO / PCBM / RbGeI_3 / CBTS / Au |
| D6 | FTO / TiO_2 / RbGeI_3 / CBTS / Au |
| D7 | FTO / PCBM / RbGeI_3 / Spiro-OMeTAD / Au |
| D8 | FTO / TiO_2 / RbGeI_3 / Spiro-OMeTAD / Au |

Table 2. Initial photovoltaic performance of the eight screened device configurations, simulated at an absorber thickness of 400 nm. Selected as the baseline for full parametric optimization.

| Dev. | Architecture | V_OC (V) | J_SC (mA/cm^2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- | --- |
| D1 | FTO/PCBM/RbGeI_3/NiO/Au | 0.81 | 30.10 | 83.68 | 20.40 |
| D2 | FTO/TiO_2/RbGeI_3/NiO/Au | 0.82 | 30.46 | 84.48 | 21.10 |
| D3 | FTO/PCBM/RbGeI_3/CuI/Au | 0.81 | 30.10 | 83.96 | 20.47 |
| D4 | FTO/TiO_2/RbGeI_3/CuI/Au | 0.81 | 30.46 | 79.98 | 19.78 |
| D5 | FTO/PCBM/RbGeI_3/CBTS/Au | 0.82 | 30.20 | 82.36 | 20.40 |
| D6 | FTO/TiO_2/RbGeI_3/CBTS/Au | 0.82 | 30.55 | 82.13 | 20.57 |
| D7 | FTO/PCBM/RbGeI_3/Spiro/Au | 0.81 | 30.07 | 85.01 | 20.71 |
| D8 | FTO/TiO_2/RbGeI_3/Spiro/Au | 0.82 | 30.46 | 83.95 | 20.97 |

Table 3. Per-step sweeps, adopted values and gate basis. Full traces: Figs. S1–S10.

| Step | Sweep range | Adopted | Gate basis |
| --- | --- | --- | --- |
| 1 thickness | 0.3–1.0 m | 0.7 m | sweep max, plateau |
| 2 bulk N_t | 1e12–1e18 cm^-3 | 1e14 | passivated-film pin (max at 1e12 shown) |
| 3 _r | 10–35 | 15 | sweep-flat pin |
| 4 | 3.7–4.2 eV | 3.9 eV | interior max (3.7 non-convergent) |
| 5/6 interface N_t | 1e12–1e18 cm^-2 | 1e14 | passivated-film pin (max at 1e12 shown) |
| 7 E_g | 1.2–1.7 eV | 1.4 eV | SQ-margin gate (max at 1.3 rejected) |
| 8 TiO_2 | 10–90 nm | 10 nm | sweep max + pinhole caveat |
| 9 CuI | 0.05–1.9 m | 100 nm | sweep-flat pin |
| 10/11 N_C/N_V | 1e18–1e20 cm^-3 | 1e18 | literature floor (sub-floor 0.13 pp) |

Table 4. Optimized material parameters of the proposed FTO/

| Parameter | TiO_2 | FTO | RbGeI_3 | CuI |
| --- | --- | --- | --- | --- |
| Thickness (nm) | 10 | 500 | 700 | 100 |
| Bandgap E_g (eV) | 3.2 | 3.2 | 1.4 | 3.1 |
| Electron affinity (eV) | 4.0 | 4.4 | 3.9 | 2.1 |
| Dielectric permittivity | 9 | 9 | 15 | 6.5 |
| CB effective DOS N_C (cm^-3) | 210^18 | 2.210^18 | 110^18 | 2.810^19 |
| VB effective DOS N_V (cm^-3) | 1.810^19 | 1.810^19 | 110^18 | 110^19 |
| Electron mobility e (cm^2 V^-1 s^-1) | 20 | 20 | 28.6 | 100 |
| Hole mobility p (cm^2 V^-1 s^-1) | 10 | 10 | 27.3 | 43.9 |
| Donor density N_D (cm^-3) | 910^16 | 110^19 | 110^9 | 0 |
| Acceptor density N_A (cm^-3) | 0 | 0 | 110^9 | 110^18 |
| Bulk defect density N_t (cm^-3) | 110^15 | 110^14 | 110^14 | 110^14 |

Table 5. Adopted reference device versus GA best-found point and sensitivity rows (defect rows re-simulated, Fig. 8; optics row reports PCE_1-sun

| Device | V_OC (V) | J_SC (mA/cm^2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- |
| Adopted reference (Table IV) | 1.06 | 30.32 | 84.11 | 27.06 |
| GA best-found (E_g 1.36 eV) | 1.04 | 31.55 | 85.87 | 28.30 |
| Reference, N_C=N_V=1e19 | 0.97 | 30.32 | 84.09 | 24.82 |
| Reference + realistic optics (0.9 sun) | 1.06 | 27.28 | 83.97 | 24.28 |

Table 6. Comparison of the proposed device with recently reported lead-free perovskite solar cells. All comparator values verified against primary sources. All entries are SCAPS-1D simulation studies.

| Device Structure | V_OC (V) | J_SC (mA/cm^2) | FF (%) | PCE (%) | Year [Ref.] |
| --- | --- | --- | --- | --- | --- |
| FTO/TiO_2/RbGeI_3/NiO/Ag | 0.5311 | 28.89 | 63.68 | 9.77 | 2022 [14] |
| FTO/TiO_2/CsGeI_3/CuI/Au | 0.667 | 22.06 | 73.49 | 10.80 | 2022 [24] |
| ITO/C_60/RbGeI_3/CBTS/Ag | 0.99 | 33.20 | 82.80 | 27.21 | 2024 [22] |
| FTO/TiO_2/RbGeI_3/PEDOT:PSS/Au | 0.813 | 30.84 | 74.19 | 18.60 | 2025 [39] |
| FTO/TiO_2/MASnI_3/CBTS/Au | 1.030 | 30.24 | 83.41 | 25.98 | 2026 [41] |
| FTO/TiO_2/MASnI_3/CZTS/Au | 0.96 | 31.66 | 67.00 | 20.36 | 2025 [42] |
| FTO/TiO_2/CsSnI_3/P3HT/Au | 0.972 | 34.70 | 78.21 | 26.38 | 2024 [40] |
| FTO/TiO_2/RbGeI_3/Spiro-OMeTAD/Au | 1.1813 | 26.31 | 85.16 | 26.47 | 2026 [23] |
| FTO/TiO_2/RbGeI_3/CuI/Au (this work) | 1.06 | 30.32 | 84.11 | 27.06 | This work |
| FTO/TiO_2/RbGeI_3/Cu_2O-BSF/CuI/Au (this work) | 1.09 | 30.32 | 84.62 | 28.01 | This work |

Table 7. RbGeI_3

| Device | Condition | V_OC (V) | J_SC (mA/cm^2) | PCE (%) |
| --- | --- | --- | --- | --- |
| RbGeI_3 | Ideal (N_t=1e14) | 1.06 | 30.32 | 27.06 |
| CsGeI_3 | Ideal (N_t=1e14) | 1.10 | 23.18 | 19.65 |
| RbGeI_3 | Realistic (N_t=1e15) | 1.02 | 30.31 | 24.40 |
| CsGeI_3 | Realistic (N_t=1e15) | 1.10 | 23.17 | 19.31 |
| RbGeI_3 | High oxidation (N_t=1e16) | 0.96 | 30.22 | 20.76 |
| CsGeI_3 | High oxidation (N_t=1e16) | 1.09 | 23.10 | 17.07 |

Table 8. Calibration check: SCAPS rebuild vs measured -CsPbI_3

| Device | V_OC (V) | J_SC (mA/cm^2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- |
| Wang control (measured) | 1.05 | 20.03 | 72.0 | 15.10 |
| SCAPS rebuild + R_s 6.9 | 1.060 | 19.92 | 71.88 | 15.18 |
| Wang champion (measured) | 1.11 | 20.0 | 82.0 | 18.40 |
| SCAPS rebuild | 1.127 | 19.92 | 82.37 | 18.49 |